# NUCLEAR THERMODYNAMIC DATABASE

# « NUCLEA »

# O-U-Zr-Fe-Cr-Ni-Ag-In-B-C-Ba-La-Ru-Sr-Al-Ca-Mg-Si

# +

# Ar-H

# - Version 2006-01 -

6, rue du Tour de l’Eau - 38400 SAINT MARTIN D'HERES - France

Téléphone : (+33) 4 76 42 76 90 - Télécopie : (+33) 4 76 63 15 37

ASBL ( loi 1901 ) - Siret : 304 441 090 00020 - NAF : 731 Z - TVA : FR 91 304 441 090

NUCLEA

Nuclear Thermodynamic Database

Version 2006-01

developed by

THERMODATA - INPG - CNRS

&

AEA-Technology

editor

B. Cheynet

scientific board

P.Chaud, P-Y. Chevalier, E. Fischer, P. Mason, M. Mignanelli.

sponsoring

AEA-T, CNRS, EURATOM, INPG, IRSN, THERMODATA

© THERMODATA 2003-2006

Copyright

The database and his documentation are protected by the French Law no 98-536 (1st July 1998), transposing the Directive 96/9/EC of the European Parliament and the Council of 11 March 1996 on the legal protection of databases.

Extraction and/or re-utilization of the whole or of a substantial part, evaluated qualitatively and/or quantitatively, is strictly prohibited.

"Extraction" means the permanent or temporary transfer of all or a substantial part of the contents to another medium by any means or in any form.

"Re-utilization" means any form of making available to the public all or a substantial part of the contents by the distribution of copies, by renting, by on-line or other forms of transmission.

The user is not allowed to make changes or amendments to the database. Completeness and intactness have to be respected.

Disclaimer

The data have been carefully evaluated by experts, they have been checked, but THERMODATA can give no guarantee for the correctness of the data provided. In any important research, results should be carefully examined and rechecked before final conclusions are drawn.

### CONTENTS

Page

#### 1.	INTRODUCTION	5

#### 2.	GENERAL DESCRIPTION	6

#### PURE COMPONENTS	6

#### CONDENSED SOLUTION PHASES	6

#### CONDENSED SUBSTANCES	6

#### GASEOUS SPECIES	6

#### 3. 	STATE of VALIDATION	24

#### BINARY AND PSEUDO-BINARY SYSTEMS	25

#### 3.2.	SELECTED TERNARY AND PSEUDO-TERNARY SYSTEMS.	26

#### 3.3.	DOMAIN OF APPLICATION AND LIMITATIONS	26

#### 3.4.	FUTURE	28

#### 4. 	ASSESSMENT of FE-O-U-ZR	29

#### 4.1	BINARY SYSTEMS	29

#### 4.2.	PSEUDO-BINARY SYSTEMS.	29

#### 4.3.	TERNARY SYSTEMS	29

I.	INTRODUCTION

Since 1990 some people were interested in the assessment of thermodynamical data for a number of compounds of reactor materials and fission products based on the recommendations of a specialists meeting held at JRC-Ispra, Italy in 1990 [*]. Critical assessments have been made on a very large number of compounds and systems. NUCLEA is a Thermodynamic Data Base built for collecting all this knowledge.

NUCLEA

is a thermodynamic database for in and ex-vessel applications containing 18 + 2 elements :

O-U-Zr-Ag-In-B-C-Fe-Cr-Ni-Ba-La-Sr-Ru-Al-Ca-Mg-Si + Ar-H

and including the 15 oxide system :

UO2-ZrO2-In2O3-B2O3-FeO-Fe2O3-Cr2O3-NiO-BaO-La2O3-OSr-Al2O3-CaO-MgO-SiO2

This database has to cover the entire field from metal to oxide domains. It allows the user to calculate the thermochemical equilibrium state at any step of a severe accident and to use the results of the thermodynamic approach for improving the predictions of thermo-hydraulic or other accidents codes.

The Gibbs energy of all possible multicomponent condensed or gaseous substances and solution phases are modelled. The binary and ternary Gibbs energy parameters were critically assessed by means of sophisticated optimisation procedures.

Applications of a global thermodynamic approach, i.e. the simultaneous use of a high-quality thermodynamic database and an equilibrium calculation code, are numerous :

- condensed state phase diagrams, transitions, liquidus/solidus, compositions and proportions,

- coupling thermodynamics and thermo-hydraulic, viscosity, segregation, residual power distribution,

- gaseous fission products release in any external conditions …

Such a database in much more than a compilation of thermodynamic data from various sources, its constitution needs a considerable work for self-consistency analysis, to ensure that all the available experimental information is satisfactorily reproduced.

Updating and improving the database has to be a regular task, tightly linked to the needs of end-users.

[*]	Fission Product Chemistry in Severe Nuclear Reactor Accidents, Specialist’s Meeting at JRC-Ispra, 15-17 January 1990, EUR 12989 EN (1990), A.L. Nichols ed.

2.	GENERAL DESCRIPTION

2.1.	PURE COMPONENTS.

The NUCLEA Thermodynamic Database for In- and Ex-Vessel Applications contains the 18 + 2 following elements :

O-U-Zr-Fe-Cr-Ni-Ag-In-B-C-Ba-La-Ru-Sr-Al-Ca-Mg-Si + Ar-H.

Ar and H are not taken into account in condensed solution phases.

# 2.2.	CONDENSED SOLUTION PHASES.

The condensed solutions (48 non-stoichiometric phases, based on 281 reference substances) were deduced from the analysis of the assessed sub-systems (binary, ternary, …) ; some of them present possible miscibility gaps.

The list of condensed solutions stored in NUCLEA is presented in table 1.

2.3.	CONDENSED SUBSTANCES.

The condensed stoechiometric compounds are presented in table 2.

Hydrogen was added because it is a major component of the system, but the dissolution of hydrogen in condensed solid and liquid solutions is not taken into account at this time.

2.4.	GASEOUS SPECIES.

The gaseous species were added as an ideal mixture. The list is presented in table 3.

Table 1	Condensed solution phases stored in NUCLEA

N°	NAME	ELEMENTS 	TYPE	MG  	TMAX

1	LIQUID	Ag, Al, B, Ba, C, Ca, Cr, Fe, In, 	MOC	1

La, Mg, Ni, O, Ru, Si, Sr, U, Zr

2	FCC_C1	O, U, Zr, Ba, Ca, In, La, Mg, Sr	O	1	3120

3	TET(OXIDE)	O, U, Zr, In, Mg		O	0	2650

4	PEROVSKIT1	O, Ba, Sr, U, Zr		O	0	3023

5	FCC_B1(4)	C, U, Zr, O 		MOC	1	3200

6	BCT	C, O, U		MOC	0	2100

7	B4C	B, C		C	0	2800

8	BCC_A2(1)	Fe, Cr, Ni, C, Ru, In, U, Zr	MC	0	2180

9	BCC_A2(2)	U, Zr, O, Ag, C, Fe, In, Ru, Cr, Ni	MOC	1	2250

10	FCC_A1(1)	Fe, Cr, Ni, Ru, In, Al, Zr, C	MC	0	1800

11	HCP_A3(1)	Ru, Zr, O, C, Ag, Al, In, 	MOC	1	2607

Fe, Cr, Mg, Ni, U

12	LAVES	Cr, Fe, U, Zr		M	1	1947

13	FCC_B1(1)	Fe, O, Sr, Ca, Mg, Ni		O	0	1650

14	FCC_B1(2)	Mg, Ni, O, Cr, Fe, Ca		O	0	3100

15	FCC_B1(3)	Ba, Ca, Sr, O, Fe, Mg, Ni		O	1	3172

16	RHO	Al, Cr, Fe, O		O	1	2603

17	SPINEL	Al, Cr, Fe, O, Mg, Ni		O	0	2500

18	CC	La, O, Ba, Ca, Sr, Zr		O	0	2586

19	TCHERNO	O, U, Zr, Si		O	0	1910

20	MULLITE	Al, B, O, Si		O	0	2200

21	M7C3	C, Cr, Fe, Ni		MC	0	2100

22	M23C6(1)	C, Cr, Fe, Ni		MC	0	1900

23	M3C	B, C, Cr, Fe, Ni		MC	0	1600

24	C2La(H_T)	C, La		MC	0	2800

25	C3La2(S)	C, La		MC	0	1700

26	BETA_B	B, Si	M	0	2000

27	DIA_A4	Si, B, Ru	M	0	1687

28	FCC_A1(2)	Ag, Al, In, Mg	M	0	1235

29	HCP_A3(3)	In, Ni	M	0	1210

30	BCC_A2(5)	In, Ni	M	0	1200

31	M23C6(2)	B, C, Fe	MC	0	1200

32	BCC_A2(4)	La, In, Ag, C, Ca, Mg	MC	0	1193

33	FCC_A1(4)	La, In, Ag, Ba, C, Ca, Mg	MC	0	1134

34	BCC_A2(3)	Ba, Ca, Sr	M	0	1115

35	SIGMA	Cr, Fe, Ni		M	0	1088

36	BCC_A2(6)	Ag, Al, In, Mg	M	0	1052

37	TET(METAL)	U, Ru, Zr, Cr, Fe, Al, Si		M	0	1049

38	HCP_A3(2)	Ag, Al, In	M	0	1008

39	ORT_A20	U, Zr, Fe		M	0	942

40	DELTA	U, Zr		M	0	900

41	FCC_A1(3)	Sr, Ba, Ca, La	M	0	820

42	BCC_A12	Al, Mg	M	0	734

43	CUB_A13	Ag, Al	M	0	732

44	FCC_L10	In, Mg	M	0	630

45	FCC_L12	In, Mg	M	0	611

46	TET_A6	In, Mg	M	0	440

47	CW2S_Olivine	Ca, Fe, Si, O	O	0

48	CWS_Wollastonite	Ca, Fe, Si, O	O	0

NOTE :

TMAX	maximal stability temperature.	M	metallic.

MG	miscibility gap index.	O	oxide.

C	carbon.

Table 2	Condensed stoichiometric compounds stored in NUCLEA.

Gibbs energy at  T = 298.15 K

N°	SUBSTANCES                        	     J / mole    	   J / g-atom

| 1 |  | AG1(SER) | 0 | 0 |
| --- | --- | --- | --- | --- |
| 2 |  | AG1BA1(S) | -65411.64 | -32705.82 |
| 3 |  | AG1CA1(S) | -74932.67 | -37466.34 |
| 4 |  | AG1CA3(S) | -108103.23 | -27025.81 |
| 5 |  | AG1IN2(S) | -58960.17 | -19653.39 |
| 6 |  | AG1LA1(S) | -82861.57 | -41430.79 |
| 7 |  | AG1MG3(S) | -123785.78 | -30946.45 |
| 8 |  | AG1SR1(S) | -86085.06 | -43042.53 |
| 9 |  | AG1ZR1(S) | -34539.29 | -17269.64 |
| 10 |  | AG1ZR2(S) | -52746.23 | -17582.08 |
| 11 |  | AG2BA1(S) | -99075.38 | -33025.13 |
| 12 |  | AG2BA3(S) | -150615.45 | -30123.09 |
| 13 |  | AG2C1O3(S) | -560775.27 | -93462.54 |
| 14 |  | AG2CA1(S) | -104725.47 | -34908.49 |
| 15 |  | AG2CR1O4(S) | -786189.5 | -112312.79 |
| 16 |  | AG2IN1(S) | -64975.33 | -21658.44 |
| 17 |  | AG2LA1(S) | -119443.83 | -39814.61 |
| 18 |  | AG2O1(S) | -66844.27 | -22281.42 |
| 19 |  | AG2SR1(S) | -122606.57 | -40868.86 |
| 20 |  | AG2SR3(S) | -205646.79 | -41129.36 |
| 21 |  | AG3CA5(S) | -266950.98 | -33368.87 |
| 22 |  | AG3IN1(S) | -82025.94 | -20506.48 |
| 23 |  | AG3MG1(S) | -95984.28 | -23996.07 |
| 24 |  | AG46LA14(S) | -2191519.87 | -36525.33 |
| 25 |  | AG4SR1(S) | -161549.45 | -32309.89 |
| 26 |  | AG5BA1(S) | -149298.93 | -24883.15 |
| 27 |  | AG5LA1(S) | -179645.45 | -29940.91 |
| 28 |  | AG5SR1(S) | -180007.11 | -30001.18 |
| 29 |  | AG7CA2(S) | -287830.51 | -31981.17 |
| 30 |  | AG9CA2(S) | -318585.56 | -28962.32 |
| 31 |  | AL1(SER) | 0 | 0 |
| 32 |  | AL11LA1O18(S) | -10292251.95 | -343075.07 |
| 33 |  | AL11LA3(S) | -681472.96 | -48676.64 |
| 34 |  | AL12BA1O19(S) | -10946776.01 | -342086.75 |
| 35 |  | AL12CA1O19(S) | -10824390.41 | -338262.2 |
| 36 |  | AL12O19SR1(S) | -10867144.19 | -339598.26 |
| 37 |  | AL13BA7(S) | -667889.54 | -33394.48 |
| 38 |  | AL13CR2(S) | -310025.98 | -20668.4 |
| 39 |  | AL13RU4(S) | -832218.53 | -48954.03 |
| 40 |  | AL14CA12O33(S) | -19722849.59 | -334285.59 |
| 41 |  | AL1B10(S) | -132380.35 | -12034.58 |
| 42 |  | AL1B12(S) | -190235.86 | -14633.53 |
| 43 |  | AL1B2(S) | -55416.53 | -18472.18 |
| 44 |  | AL1CR2(S) | -58903.03 | -19634.34 |
| 45 |  | AL1FE1O3(S) | -1264202.16 | -252840.43 |
| 46 |  | AL1H3(S) | -20238.22 | -5059.55 |
| 47 |  | AL1H3O3(S)A | -1297326.81 | -185332.4 |
| 48 |  | AL1LA1(S) | -102389.06 | -51194.53 |
| 49 |  | AL1LA1O3(S) | -1818974.18 | -363794.84 |
| 50 |  | AL1LA3(S) | -139527.19 | -34881.8 |
| 51 |  | AL1NI3(S) | -214739.17 | -53684.79 |
| 52 |  | AL1RU1(S) | -134994.02 | -67497.01 |
| 53 |  | AL1SR1(S) | -86239.73 | -43119.87 |
| 54 |  | AL1ZR1(S) | -109067.05 | -54533.52 |
| 55 |  | AL1ZR2(S) | -138502.46 | -46167.49 |
| 56 |  | AL1ZR3(S) | -151961.76 | -37990.44 |
| 57 |  | AL24LA10(S) | -1775265.06 | -52213.68 |
| 58 |  | AL2BA1O4(S) | -2385338.43 | -340762.63 |
| 59 |  | AL2BA3O6(S) | -3583289.8 | -325753.62 |
| 60 |  | AL2CA1(S) | -122134.47 | -40711.49 |
| 61 |  | AL2CA1H4O10SI2(S) | -4929367.36 | -259440.39 |
| 62 |  | AL2CA1O4(S) | -2360141.15 | -337163.02 |
| 63 |  | AL2CA1O8SI2(ANORTHITE) | -4286579.18 | -329736.86 |
| 64 |  | AL2CA1SI2(S) | -229256.91 | -45851.38 |
| 65 |  | AL2CA2O7SI1(MELILITE) | -4048152.09 | -337346.01 |
| 66 |  | AL2CA3H12O12(S) | -5625109.76 | -193969.3 |
| 67 |  | AL2CA3O6(S) | -3646856.78 | -331532.43 |
| 68 |  | AL2CA4H26O20(S) | -8503547.37 | -163529.76 |
| 69 |  | AL2FE1(S) | -95777.24 | -31925.75 |
| 70 |  | AL2H2O4(S)B | -2009584.81 | -251198.1 |
| 71 |  | AL2H2O4(S)D | -2020184.66 | -252523.08 |
| 72 |  | AL2H4O9SI2(S)D | -4177066.75 | -245709.81 |
| 73 |  | AL2H4O9SI2(S)H | -4161813.19 | -244812.54 |
| 74 |  | AL2H4O9SI2(S)K | -4156804.1 | -244517.89 |
| 75 |  | AL2H6O6(S) | -2628338.7 | -187738.48 |
| 76 |  | AL2LA1(S) | -157750.02 | -52583.34 |
| 77 |  | AL2O4SR1(H_T) | -2374296.7 | -339185.24 |
| 78 |  | AL2O4SR1(L_T) | -2375742.84 | -339391.83 |
| 79 |  | AL2O6SR3(S) | -3617906.48 | -328900.59 |
| 80 |  | AL2RU1(S) | -169593.03 | -56531.01 |
| 81 |  | AL2SR1(S) | -144823.56 | -48274.52 |
| 82 |  | AL2U1(S) | -125462.65 | -41820.88 |
| 83 |  | AL2ZR1(S) | -163662.05 | -54554.02 |
| 84 |  | AL2ZR3(S) | -254369.78 | -50873.96 |
| 85 |  | AL32O132SR84(S) | -79479655.53 | -320482.48 |
| 86 |  | AL3FE1(S) | -132431.35 | -33107.84 |
| 87 |  | AL3FE2(S) | -126493.92 | -25298.78 |
| 88 |  | AL3LA1(S) | -211212.63 | -52803.16 |
| 89 |  | AL3NI1(S) | -183167.43 | -45791.86 |
| 90 |  | AL3NI2(S) | -315869.83 | -63173.97 |
| 91 |  | AL3RU2(S) | -292431.72 | -58486.34 |
| 92 |  | AL3U1(S) | -159033.48 | -39758.37 |
| 93 |  | AL3ZR1(S) | -196422.78 | -49105.7 |
| 94 |  | AL3ZR2(S) | -280101.93 | -56020.39 |
| 95 |  | AL3ZR5(S) | -393057.27 | -49132.16 |
| 96 |  | AL4B2O9(S) | -4689569.94 | -312638 |
| 97 |  | AL4BA1(S) | -175953.93 | -35190.79 |
| 98 |  | AL4C3(S) | -246315.48 | -35187.93 |
| 99 |  | AL4C4SI1(S) | -333137.35 | -37015.26 |
| 100 |  | AL4CA1(S) | -139548.5 | -27909.7 |
| 101 |  | AL4CA1O7(S) | -4051114.86 | -337592.91 |
| 102 |  | AL4CR1(S) | -122910.94 | -24582.19 |
| 103 |  | AL4MG2O18SI5(S) | -9223667.76 | -318057.51 |
| 104 |  | AL4O7SR1(S) | -4092161.04 | -341013.42 |
| 105 |  | AL4SR1(S) | -246166.23 | -49233.25 |
| 106 |  | AL4U0.9(S) | -162010.38 | -33063.34 |
| 107 |  | AL4ZR5(S) | -481032.75 | -53448.08 |
| 108 |  | AL525MG475(S) | -10803297.58 | -10803.3 |
| 109 |  | AL56MG44(S) | -1062236.3 | -10622.36 |
| 110 |  | AL5BA4(S) | -284913.42 | -31657.05 |
| 111 |  | AL5FE2(S) | -228653.05 | -32664.72 |
| 112 |  | AL6RU1(S) | -243344.11 | -34763.44 |
| 113 |  | AL8C7SI1(S) | -596661.56 | -37291.35 |
| 114 |  | AL8CR5(S) | -304868.55 | -23451.43 |
| 115 |  | AL8MG5(S) | -140899.19 | -10838.4 |
| 116 |  | AL9CR4(S) | -311799.61 | -23984.59 |
| 117 |  | B1(SER) | 0 | 0 |
| 118 |  | B10H14(C) | -81541.36 | -3397.56 |
| 119 |  | B12U1(S) | -449523.87 | -34578.76 |
| 120 |  | B12ZR1(S) | -298738.29 | -22979.87 |
| 121 |  | B14SI1(S) | -138034.11 | -9202.27 |
| 122 |  | B1C1U1(S) | -183438.29 | -61146.1 |
| 123 |  | B1CR1(S) | -83531.44 | -41765.72 |
| 124 |  | B1CR2(S) | -109036.77 | -36345.59 |
| 125 |  | B1FE1(S) | -70601.46 | -35300.73 |
| 126 |  | B1FE1O3(S) | -1073456.08 | -214691.22 |
| 127 |  | B1FE2(S) | -81124.73 | -27041.58 |
| 128 |  | B1FE3O6(S) | -1908717.79 | -190871.78 |
| 129 |  | B1H1O2(C) | -817378.52 | -204344.63 |
| 130 |  | B1H3O3(S) | -1120457.85 | -160065.41 |
| 131 |  | B1NI1(S) | -47073.99 | -23537 |
| 132 |  | B1NI2(S) | -81887.88 | -27295.96 |
| 133 |  | B1NI3(S) | -94450.22 | -23612.56 |
| 134 |  | B1O1.5(S) | -644793.39 | -257917.36 |
| 135 |  | B1RU1(S) | -55899.88 | -27949.94 |
| 136 |  | B1ZR1(S) | -176509.51 | -88254.75 |
| 137 |  | B2BA1O4(S) | -2001383.44 | -285911.92 |
| 138 |  | B2BA3O6(S) | -3156115.24 | -286919.57 |
| 139 |  | B2C1U1(S) | -230197.37 | -57549.34 |
| 140 |  | B2C7U5(S) | -780338.33 | -55738.45 |
| 141 |  | B2CA1O4(S) | -2062745.48 | -294677.93 |
| 142 |  | B2CA1O8SI2(S) | -3905837.29 | -300449.02 |
| 143 |  | B2CA2O5(S) | -2778261.49 | -308695.72 |
| 144 |  | B2CA3O6(S) | -3484066.61 | -316733.33 |
| 145 |  | B2CA5O10SI1(S) | -5838977.86 | -324387.66 |
| 146 |  | B2CR1(S) | -129261.02 | -43087.01 |
| 147 |  | B2FE1O4(S) | -1579891.28 | -225698.75 |
| 148 |  | B2FE2O5(S) | -1870208.54 | -207800.95 |
| 149 |  | B2FE3O6(S) | -2160504.75 | -196409.52 |
| 150 |  | B2FE3U1(S) | -234009.51 | -39001.59 |
| 151 |  | B2H4O4(S) | -1447850.19 | -144785.02 |
| 152 |  | B2IN2O6(S) | -2274346.65 | -227434.66 |
| 153 |  | B2LA2O6(S) | -3200888.71 | -320088.87 |
| 154 |  | B2LA6O12(S) | -6875312.02 | -343765.6 |
| 155 |  | B2MG1(S) | -85027.23 | -28342.41 |
| 156 |  | B2MG2O5(S) | -2586983.82 | -287442.65 |
| 157 |  | B2MG3O6(S) | -3210718.06 | -291883.46 |
| 158 |  | B2NI2O5(S) | -1786882.29 | -198542.48 |
| 159 |  | B2NI3O6(S) | -2684614.08 | -244055.83 |
| 160 |  | B2O4SR1(S) | -2039632.42 | -291376.06 |
| 161 |  | B2O5SR2(S) | -2693841.04 | -299315.67 |
| 162 |  | B2O6SR3(S) | -3345079.69 | -304098.15 |
| 163 |  | B2RU1(S) | -64529.78 | -21509.93 |
| 164 |  | B2U1(S) | -180686.63 | -60228.88 |
| 165 |  | B2ZR1(S) | -332977.04 | -110992.35 |
| 166 |  | B3CR5(S) | -305745.69 | -38218.21 |
| 167 |  | B3H3O3(S) | -1312211.18 | -145801.24 |
| 168 |  | B3NI4(S) | -180515.06 | -25787.87 |
| 169 |  | B3RU2(S) | -117375.7 | -23475.14 |
| 170 |  | B3RU7(S) | -248863.36 | -24886.34 |
| 171 |  | B3SI1(S) | -40318.35 | -10079.59 |
| 172 |  | B4BA1O7(S) | -3353866.05 | -279488.84 |
| 173 |  | B4CA1O7(S) | -3401581.06 | -283465.09 |
| 174 |  | B4CR1(S) | -143702.66 | -28740.53 |
| 175 |  | B4CR3(S) | -300194.72 | -42884.96 |
| 176 |  | B4FE1U1(S) | -323844.87 | -53974.15 |
| 177 |  | B4LA1(S) | -336133.98 | -67226.8 |
| 178 |  | B4MG1(S) | -109898.64 | -21979.73 |
| 179 |  | B4MG1O7(S) | -3281304.33 | -273442.03 |
| 180 |  | B4O7SR1(S) | -3383923.05 | -281993.59 |
| 181 |  | B4U1(S) | -262832.38 | -52566.48 |
| 182 |  | B4ZR3(S) | -687794.06 | -98256.29 |
| 183 |  | B5H9(L) | -12113.99 | -865.28 |
| 184 |  | B6BA1(S) | -139573.03 | -19939 |
| 185 |  | B6CA1(S) | -130370.27 | -18624.32 |
| 186 |  | B6LA1(S) | -495419.13 | -70774.16 |
| 187 |  | B6LA2O12(S) | -5805804.43 | -290290.22 |
| 188 |  | B6O10SR1(S) | -4715632.16 | -277390.13 |
| 189 |  | B6SI1(S) | -68841.13 | -9834.45 |
| 190 |  | B6SR1(S) | -146468.5 | -20924.07 |
| 191 |  | B7MG1(S) | -144815.93 | -18101.99 |
| 192 |  | B8BA1O13(S) | -6022469.4 | -273748.61 |
| 193 |  | B9LA1(S) | -513384.79 | -51338.48 |
| 194 |  | BA1(SER) | 0 | 0 |
| 195 |  | BA13IN1(S) | -337548.7 | -24110.62 |
| 196 |  | BA1C1O3(C) | -1244422.84 | -248884.57 |
| 197 |  | BA1C2(S) | -109126.62 | -36375.54 |
| 198 |  | BA1CR1O4(S) | -1493281.05 | -248880.18 |
| 199 |  | BA1CR2O4(S) | -1799480.43 | -257068.63 |
| 200 |  | BA1FE12O19(S) | -5768158.27 | -180254.95 |
| 201 |  | BA1FE2O4(S) | -1502694.8 | -214670.69 |
| 202 |  | BA1H2(C) | -208883.49 | -69627.83 |
| 203 |  | BA1H2O2(C) | -972184.89 | -194436.98 |
| 204 |  | BA1IN1(S) | -94163.39 | -47081.7 |
| 205 |  | BA1IN2(S) | -150651.48 | -50217.16 |
| 206 |  | BA1IN2O4(S) | -1568262.02 | -224037.43 |
| 207 |  | BA1IN4(S) | -213763.29 | -42752.66 |
| 208 |  | BA1LA2O4(S) | -2624374.86 | -374910.69 |
| 209 |  | BA1MG2(S) | -65742.96 | -21914.32 |
| 210 |  | BA1NI1O2(S) | -851801.03 | -212950.26 |
| 211 |  | BA1O2(S) | -666582.79 | -222194.26 |
| 212 |  | BA1O3SI1(S) | -1653860.2 | -330772.04 |
| 213 |  | BA1O4U1(S) | -2043006.15 | -340501.03 |
| 214 |  | BA1O5SI2(S) | -2587876.91 | -323484.61 |
| 215 |  | BA1SI1(S) | -174914.37 | -87457.19 |
| 216 |  | BA1SI2(S) | -243646.07 | -81215.36 |
| 217 |  | BA2FE2O5(S) | -2128609.36 | -236512.15 |
| 218 |  | BA2FE6O11(S) | -3873018.41 | -203843.07 |
| 219 |  | BA2IN2O5(S) | -2154375.78 | -239375.09 |
| 220 |  | BA2MG17(S) | -303668.58 | -15982.56 |
| 221 |  | BA2O4SI1(S) | -2327410.02 | -332487.15 |
| 222 |  | BA2O8SI3(S) | -4258753.65 | -327596.43 |
| 223 |  | BA3CR2O6(S) | -3029858.54 | -275441.69 |
| 224 |  | BA3IN2O6(S) | -2728999.89 | -248090.9 |
| 225 |  | BA3NI1O4(S) | -2015105.41 | -251888.18 |
| 226 |  | BA3O13SI5(S) | -6848913.41 | -326138.73 |
| 227 |  | BA4IN6O13(S) | -5296598.63 | -230286.9 |
| 228 |  | BA5IN2(S) | -268810.05 | -38401.44 |
| 229 |  | BA5IN2O8(S) | -3873125.74 | -258208.38 |
| 230 |  | BA5IN3(S) | -344383.03 | -43047.88 |
| 231 |  | BA5O21SI8(S) | -11109843.47 | -326760.1 |
| 232 |  | BA6MG23(S) | -544661.97 | -18781.45 |
| 233 |  | BA7FE4O13(S) | -6074799.94 | -253116.66 |
| 234 |  | C1(GRA_HEX_A9) | -1712.07 | -1712.07 |
| 235 |  | C1(SER) | 0 | 0 |
| 236 |  | C1CA1O3(C) | -1233944.31 | -246788.86 |
| 237 |  | C1FE1O3(S) | -768261.6 | -153652.32 |
| 238 |  | C1H2O2(L) | -461252.38 | -92250.48 |
| 239 |  | C1H4(L) | -117191.52 | -23438.3 |
| 240 |  | C1H4O1(L) | -276758.56 | -46126.43 |
| 241 |  | C1MG1O3(C) | -1131323.81 | -226264.76 |
| 242 |  | C1NI1O3(S) | -705348.18 | -141069.64 |
| 243 |  | C1O3SR1(C) | -1255980.02 | -251196 |
| 244 |  | C1O5U1(S) | -1732405.91 | -247486.56 |
| 245 |  | C1SI1(S) | -75564.13 | -37782.07 |
| 246 |  | C2CA1(S) | -84419.43 | -28139.81 |
| 247 |  | C2CA1MG1O6(S) | -2361482.36 | -236148.24 |
| 248 |  | C2CR3(M3C2)(C-CR-FE-NI) | -85077.34 | -17015.47 |
| 249 |  | C2H4O2(L) | -527955.84 | -65994.48 |
| 250 |  | C2H6(L) | -144893.31 | -18111.66 |
| 251 |  | C2H6O1(L) | -324837.85 | -36093.09 |
| 252 |  | C2H6O2(L) | -512930.67 | -51293.07 |
| 253 |  | C2LA1(LT) | -88411.03 | -29470.34 |
| 254 |  | C2MG1(S) | 71647.03 | 23882.34 |
| 255 |  | C2SR1(S) | -105723.58 | -35241.19 |
| 256 |  | C3H6(L) | 34388.3 | 3820.92 |
| 257 |  | C3H6O1(L) | -308062.61 | -30806.26 |
| 258 |  | C3H6O2(L) | -564656.5 | -51332.41 |
| 259 |  | C3H8(L) | -180280.25 | -16389.11 |
| 260 |  | C3H8O1(L) | -360193.89 | -30016.16 |
| 261 |  | C3H8O3(L) | -723497.9 | -51678.42 |
| 262 |  | C3MG2(S) | 45372.97 | 9074.59 |
| 263 |  | C3U2(S) | -231519 | -46303.8 |
| 264 |  | C4NI1O4(L) | -727061.22 | -80784.58 |
| 265 |  | C5FE1O5(L) | -866589.79 | -78780.89 |
| 266 |  | C6CR1O6(S) | -1171064.1 | -90081.85 |
| 267 |  | CA1(SER) | 0 | 0 |
| 268 |  | CA1CR2O4(S) | -1839001.87 | -262714.55 |
| 269 |  | CA1FE1O6SI2(hedenbergite) | -2897011.83 | -289701.18 |
| 270 |  | CA1FE2O4(S) | -1523966.95 | -217709.56 |
| 271 |  | CA1FE3O5(S)(CWF) | -1799227.2 | -199914.13 |
| 272 |  | CA1FE4O7(S) | -2318781.61 | -193231.8 |
| 273 |  | CA1FE5O7(S)(CW3F) | -2332531.66 | -179425.51 |
| 274 |  | CA1H2(C) | -189343.35 | -63114.45 |
| 275 |  | CA1H2O2(S) | -1010946.99 | -202189.4 |
| 276 |  | CA1H4O7SI2(S) | -3189857.9 | -227846.99 |
| 277 |  | CA1IN1(S) | -108855.4 | -54427.7 |
| 278 |  | CA1IN2(S) | -151862.11 | -50620.7 |
| 279 |  | CA1MG1O2(S) | -1262837.85 | -315709.46 |
| 280 |  | CA1MG1O4SI1(S) | -2293553.05 | -327650.44 |
| 281 |  | CA1MG1O6SI2(S) | -3242583.18 | -324258.32 |
| 282 |  | CA1MG2(S) | -67601.02 | -22533.67 |
| 283 |  | CA1NI2(S) | -82617.09 | -27539.03 |
| 284 |  | CA1NI3(S) | -99850.58 | -24962.64 |
| 285 |  | CA1NI5(S) | -123283.62 | -20547.27 |
| 286 |  | CA1O2(S) | -683929.19 | -227976.4 |
| 287 |  | CA1O3SI1(PSEUDOWOL)(ASS1) | -1654867.65 | -330973.53 |
| 288 |  | CA1O3ZR1(S) | -1793173.43 | -358634.69 |
| 289 |  | CA1O4U1(S) | -2040940.74 | -340156.79 |
| 290 |  | CA1SI1(S) | -121183.8 | -60591.9 |
| 291 |  | CA1SI2(S) | -167426.9 | -55808.97 |
| 292 |  | CA2FE2O5(S) | -2185331.96 | -242814.66 |
| 293 |  | CA2H2.333O5.166SI1(S) | -2713528.85 | -258455.93 |
| 294 |  | CA2H2MG5O24SI8(S) | -12509475 | -305109.15 |
| 295 |  | CA2H5O10.5SI3(S) | -5000088.93 | -243906.78 |
| 296 |  | CA2MG1O7SI2(S) | -3935082.98 | -327923.58 |
| 297 |  | CA2NI7(S) | -212712.9 | -23634.77 |
| 298 |  | CA2O4SI1(ALPHA)(ASS1) | -2341216.25 | -334459.46 |
| 299 |  | CA2O4SI1(ALPHA2)(ASS1) | -2337492.61 | -333927.52 |
| 300 |  | CA2O4SI1(LARNITE)(ASS1) | -2344891.27 | -334984.47 |
| 301 |  | CA2SI1(S) | -145102.2 | -48367.4 |
| 302 |  | CA3H6O10SI2(S) | -4875790.89 | -232180.52 |
| 303 |  | CA3IN1(S) | -163480.62 | -40870.16 |
| 304 |  | CA3MG1O8SI2(S) | -4637291.31 | -331235.09 |
| 305 |  | CA3O5SI1(HATRURITE)(ASS1) | -2984252.16 | -331583.57 |
| 306 |  | CA3O7SI2(RANKINITE)(ASS1) | -3997993.42 | -333166.12 |
| 307 |  | CA4H3O11.5SI3(S) | -6122610.14 | -284772.56 |
| 308 |  | CA5H11O22.5SI6(S) | -10876620.22 | -244418.43 |
| 309 |  | CA5H21O27.5SI6(S) | -12420570.82 | -208749.09 |
| 310 |  | CA5H6O20SI6(S) | -10088745.72 | -272668.8 |
| 311 |  | CA6H2O19SI6(S) | -10176180.79 | -308369.11 |
| 312 |  | CR1(SER) | 0 | 0 |
| 313 |  | CR1LA1O3(S) | -1568480.14 | -313696.03 |
| 314 |  | CR1O2(S) | -596795.01 | -198931.67 |
| 315 |  | CR1O3(C) | -599685.11 | -149921.28 |
| 316 |  | CR1SI1(S)(2) | -73062.9 | -36531.45 |
| 317 |  | CR1SI2(S)(2) | -96870.6 | -32290.2 |
| 318 |  | CR2RU1(S) | -36466.85 | -12155.62 |
| 319 |  | CR3RU1(S) | -42755.49 | -10688.87 |
| 320 |  | CR3SI1(S)(2) | -152823.68 | -38205.92 |
| 321 |  | CR5O12(S) | -3023645.63 | -177861.51 |
| 322 |  | CR5SI3(S)(2) | -313618.51 | -39202.31 |
| 323 |  | CR8O21(S) | -4830650.55 | -166574.16 |
| 324 |  | FE1(SER) | 0 | 0 |
| 325 |  | FE10O22SR7(S) | -8939581.75 | -229220.04 |
| 326 |  | FE12LA1O19.5(S) | -6054445.14 | -186290.62 |
| 327 |  | FE12O19SR1(S) | -5927749.78 | -185242.18 |
| 328 |  | FE1H1O2(S) | -576696.07 | -144174.02 |
| 329 |  | FE1H2O2(S) | -600241.45 | -120048.29 |
| 330 |  | FE1H3O3(S) | -863802.49 | -123400.36 |
| 331 |  | FE1LA1O3(S) | -1404196.83 | -280839.37 |
| 332 |  | FE1O4U1(S) | -1623035.11 | -270505.85 |
| 333 |  | FE1SI1(S) | -78887.03 | -39443.51 |
| 334 |  | FE1SI2(S) | -92094.14 | -30698.05 |
| 335 |  | FE1U6(S) | -139561.05 | -19937.29 |
| 336 |  | FE1ZR2(S) | -69427.85 | -23142.62 |
| 337 |  | FE1ZR3(S) | -99821.26 | -24955.32 |
| 338 |  | FE2H2O4(S) | -1153392.65 | -144174.08 |
| 339 |  | FE2O5SR2(S) | -2176992.73 | -241888.08 |
| 340 |  | FE2O6SR3(S) | -2822811.84 | -256619.26 |
| 341 |  | FE2SI1(S) | -83713.97 | -27904.66 |
| 342 |  | FE333U250ZR417(e) | -27027.11 | -27027.11 |
| 343 |  | FE3SI7(S) | -244014.67 | -24401.47 |
| 344 |  | FE50U18ZR32(k) | -30356.85 | -30356.85 |
| 345 |  | FE5SI3(S) | -266531.65 | -33316.46 |
| 346 |  | FE6U71ZR23(l) | -17793.96 | -17793.96 |
| 347 |  | FE735ZR265(S) | -26835917.79 | -26835.92 |
| 348 |  | H2LA1(S) | -204522.91 | -68174.3 |
| 349 |  | H2MG1(S) | -85418.67 | -28472.89 |
| 350 |  | H2MG1O2(S) | -943519.35 | -188703.87 |
| 351 |  | H2MG3O12SI4(S) | -5993139.61 | -285387.6 |
| 352 |  | H2MG7O24SI8(S) | -12243019.3 | -298610.23 |
| 353 |  | H2O1(L) | -306684.99 | -102228.33 |
| 354 |  | H2O2SR1(C) | -992218.88 | -198443.78 |
| 355 |  | H2O4U1(S) | -1574966.17 | -224995.17 |
| 356 |  | H2SR1(C) | -195503.66 | -65167.89 |
| 357 |  | H2ZR1(S) | -181153.17 | -60384.39 |
| 358 |  | H3LA1O3(S) | -1447228.46 | -206746.92 |
| 359 |  | H3U1(S) | -146154.99 | -36538.75 |
| 360 |  | H4MG3O9SI2(S) | -4427808.81 | -245989.38 |
| 361 |  | H4O5U1(S) | -1876492.03 | -187649.2 |
| 362 |  | H6SI2(S) | -1856.58 | -232.07 |
| 363 |  | IN1(SER) | 0 | 0 |
| 364 |  | IN1LA1(S) | -113481.27 | -56740.63 |
| 365 |  | IN1LA2(S) | -144762.23 | -48254.08 |
| 366 |  | IN1LA3(S) | -165393.64 | -41348.41 |
| 367 |  | IN1MG2(S) | -70328.59 | -23442.86 |
| 368 |  | IN1MG3(S) | -83590 | -20897.5 |
| 369 |  | IN1NI1(S) | -67964.87 | -33982.43 |
| 370 |  | IN1NI2(S) | -82165.11 | -27388.37 |
| 371 |  | IN1NI3(S) | -93648.86 | -23412.21 |
| 372 |  | IN1SR1(S) | -80986.76 | -40493.38 |
| 373 |  | IN1SR3(S) | -118542.62 | -29635.66 |
| 374 |  | IN1ZR3(S) | -108167.48 | -27041.87 |
| 375 |  | IN2LA1(S) | -168277.47 | -56092.49 |
| 376 |  | IN2MG5(S) | -154344.28 | -22049.18 |
| 377 |  | IN2O3(S) | -953351.67 | -190670.33 |
| 378 |  | IN2O4SR1(S) | -1602215.86 | -228887.98 |
| 379 |  | IN2SR1(S) | -131339.35 | -43779.78 |
| 380 |  | IN2SR3(S) | -181434.37 | -36286.87 |
| 381 |  | IN3LA1(S) | -208827.36 | -52206.84 |
| 382 |  | IN3NI2(S) | -167579.58 | -33515.92 |
| 383 |  | IN3SR1(S) | -154657.23 | -38664.31 |
| 384 |  | IN3SR2(S) | -214884.35 | -42976.87 |
| 385 |  | IN3U1(S) | -154535.32 | -38633.83 |
| 386 |  | IN3ZR1(S) | -171584.73 | -42896.18 |
| 387 |  | IN42NI58(S) | -3111905.32 | -31119.05 |
| 388 |  | IN5LA3(S) | -459823.37 | -57477.92 |
| 389 |  | IN5SR1(S) | -195301.16 | -32550.19 |
| 390 |  | IN5SR2(S) | -286893.02 | -40984.72 |
| 391 |  | IN7MG3(S) | -221605.91 | -22160.59 |
| 392 |  | IN7NI3(S) | -316342.16 | -31634.22 |
| 393 |  | LA1(DHCP) | -16965.45 | -16965.45 |
| 394 |  | LA1(SER) | 0 | 0 |
| 395 |  | LA1MG1(S) | -39975.49 | -19987.75 |
| 396 |  | LA1MG12(S) | -163666.79 | -12589.75 |
| 397 |  | LA1MG2(S) | -55613.79 | -18537.93 |
| 398 |  | LA1MG3(S) | -72266.96 | -18066.74 |
| 399 |  | LA1NI1(S) | -83215.34 | -41607.67 |
| 400 |  | LA1NI3(S) | -159658.92 | -39914.73 |
| 401 |  | LA1NI5(S) | -208499.96 | -34749.99 |
| 402 |  | LA1RU2(S) | -174054.54 | -58018.18 |
| 403 |  | LA1SI1(S) | -162956.09 | -81478.05 |
| 404 |  | LA1SI2(S) | -205209.61 | -68403.2 |
| 405 |  | LA2MG17(S) | -257655.85 | -13560.83 |
| 406 |  | LA2NI3(S) | -211879.53 | -42375.91 |
| 407 |  | LA2NI7(S) | -346688.07 | -38520.9 |
| 408 |  | LA2O5SI1(S) | -2852303.74 | -356537.97 |
| 409 |  | LA2O5ZR1(S) | -2966288.16 | -370786.02 |
| 410 |  | LA2O7SI2(S) | -3701822.07 | -336529.28 |
| 411 |  | LA2O7ZR2(S) | -4150169.84 | -377288.17 |
| 412 |  | LA3NI1(S) | -136079.36 | -34019.84 |
| 413 |  | LA3RU1(S) | -158894.75 | -39723.69 |
| 414 |  | LA3SI2(S) | -413874.91 | -82774.98 |
| 415 |  | LA4O12SI3(S) | -6475491.16 | -340815.32 |
| 416 |  | LA4O7SR1(S) | -4130654.4 | -344221.2 |
| 417 |  | LA4O9SR3(S) | -5311300.38 | -331956.27 |
| 418 |  | LA5RU2(S) | -290549.62 | -41507.09 |
| 419 |  | LA5RU3(S) | -364435.37 | -45554.42 |
| 420 |  | LA7NI16(S) | -940192.86 | -40877.95 |
| 421 |  | LA7NI3(S) | -364718.22 | -36471.82 |
| 422 |  | LA7RU3(S) | -421715.33 | -42171.53 |
| 423 |  | MG1(SER) | 0 | 0 |
| 424 |  | MG17SR2(S) | -264181.28 | -13904.28 |
| 425 |  | MG1NI2(S) | -81659.77 | -27219.92 |
| 426 |  | MG1O3SI1(CLINOENSTATITE) | -1565424.99 | -313085 |
| 427 |  | MG1O3SI1(ENSTATITE) | -1564852.7 | -312970.54 |
| 428 |  | MG1O3SI1(PROENSTATITE) | -1556341.36 | -311268.27 |
| 429 |  | MG1O4U1(S) | -1896226.16 | -316037.69 |
| 430 |  | MG23SR6(S) | -484397.52 | -16703.36 |
| 431 |  | MG2NI1(S) | -75027.2 | -25009.07 |
| 432 |  | MG2O4SI1(FORSTERITE) | -2201234.28 | -314462.04 |
| 433 |  | MG2SI1(S) | -97942.68 | -32647.56 |
| 434 |  | MG2SR1(S) | -59205.34 | -19735.11 |
| 435 |  | MG38SR9(S) | -766325.96 | -16304.81 |
| 436 |  | NI1(SER) | 0 | 0 |
| 437 |  | NI11ZR9(S) | -1181525.32 | -59076.27 |
| 438 |  | NI1SI1(S) | -79863.4 | -39931.7 |
| 439 |  | NI1SR1(S) | -27999.23 | -13999.61 |
| 440 |  | NI1U6(S) | -193014.49 | -27573.5 |
| 441 |  | NI1ZR1(S) | -118919.31 | -59459.66 |
| 442 |  | NI1ZR2(S) | -140726.39 | -46908.8 |
| 443 |  | NI21ZR8(S) | -1570590.04 | -54158.28 |
| 444 |  | NI29SI9(LOW_T) | -1759481.9 | -46302.16 |
| 445 |  | NI2O4SI1(S) | -1435629.04 | -205089.86 |
| 446 |  | NI2SI1(S) | -132192.4 | -44064.13 |
| 447 |  | NI2U1(S) | -176222.3 | -58740.77 |
| 448 |  | NI31SI12(S) | -2015064.98 | -46861.98 |
| 449 |  | NI35SI65(S) | -3229902.04 | -32299.02 |
| 450 |  | NI3SI1(HIGH_T) | -166182.49 | -41545.62 |
| 451 |  | NI3SI1(MEDIUM_T) | -181325.53 | -45331.38 |
| 452 |  | NI3SI2(S) | -215509.64 | -43101.93 |
| 453 |  | NI3ZR1(S) | -210303.46 | -52575.86 |
| 454 |  | NI575ZR425(S) | -60481573.4 | -60481.57 |
| 455 |  | NI5U1(S) | -301273.35 | -50212.23 |
| 456 |  | NI5ZR1(S) | -249191.04 | -41531.84 |
| 457 |  | NI769U231(S) | -58767450.18 | -58767.45 |
| 458 |  | NI778U222(S) | -58338098.71 | -58338.1 |
| 459 |  | NI7U5(S) | -701163.14 | -58430.26 |
| 460 |  | NI7ZR2(S) | -455260.68 | -50584.52 |
| 461 |  | NI9U7(S) | -922100.22 | -57631.26 |
| 462 |  | O1(SER) | 0 | 0 |
| 463 |  | O2RU1(S) | -327959.62 | -109319.87 |
| 464 |  | O2SI1(CRISTOBALITE) | -920976.83 | -306992.28 |
| 465 |  | O2SI1(H_T_QUARTZ) | -922066.17 | -307355.39 |
| 466 |  | O2SI1(L_T_QUARTZ) | -923061.3 | -307687.1 |
| 467 |  | O2SI1(TRIDYMITE) | -920540.39 | -306846.8 |
| 468 |  | O2SR1(S) | -651046.78 | -217015.59 |
| 469 |  | O2ZR1(MONOCLINIC) | -1115579.43 | -371859.81 |
| 470 |  | O3SI1SR1(S) | -1662133.98 | -332426.8 |
| 471 |  | O3U1(S) | -1252455.16 | -313113.79 |
| 472 |  | O4SI1SR2(S) | -2343579.54 | -334797.08 |
| 473 |  | O4SR2ZR1(S) | -2449213.55 | -349887.65 |
| 474 |  | O5SI1SR3(S) | -2980874.43 | -331208.27 |
| 475 |  | O7SR3ZR2(S) | -4233460.37 | -352788.36 |
| 476 |  | O8U3(S) | -3657757.71 | -332523.43 |
| 477 |  | O9U4(S) | -4611611.91 | -354739.38 |
| 478 |  | RU1(SER) | 0 | 0 |
| 479 |  | RU1SI1(S) | -130342.45 | -65171.22 |
| 480 |  | RU1U2(S) | -102970.62 | -34323.54 |
| 481 |  | RU1ZR1(S) | -153269.53 | -76634.77 |
| 482 |  | RU2SI1(S) | -104989.5 | -34996.5 |
| 483 |  | RU2SI3(S) | -303896.05 | -60779.21 |
| 484 |  | RU2ZR1(S) | -140564.4 | -46854.8 |
| 485 |  | RU3U1(S) | -167385.3 | -41846.33 |
| 486 |  | RU474U526(S) | -35067025.96 | -35067.03 |
| 487 |  | RU4SI3(S) | -421958.8 | -60279.83 |
| 488 |  | RU4U3(S) | -239055.24 | -34150.75 |
| 489 |  | RU5SI3(S) | -344813.42 | -43101.68 |
| 490 |  | RU5U3(S) | -284872.9 | -35609.11 |
| 491 |  | SI1(SER) | 0 | 0 |
| 492 |  | SI1.88U1(S) | -149415.74 | -51880.47 |
| 493 |  | SI1SR1(S) | -124089.34 | -62044.67 |
| 494 |  | SI1SR2(S) | -162868.03 | -54289.34 |
| 495 |  | SI1U3(HIGH_T) | 400000 | 100000 |
| 496 |  | SI1U3(LOW_T) | -138370.03 | -34592.51 |
| 497 |  | SI1ZR1(S) | -163470.17 | -81735.09 |
| 498 |  | SI1ZR2(S) | -220471.97 | -73490.66 |
| 499 |  | SI1ZR3(S) | -256466.22 | -64116.55 |
| 500 |  | SI2SR1(S) | -158317.95 | -52772.65 |
| 501 |  | SI2U3(S) | -231732.67 | -46346.53 |
| 502 |  | SI2ZR1(S) | -174982.81 | -58327.6 |
| 503 |  | SI2ZR3(S) | -402778.02 | -80555.6 |
| 504 |  | SI3U1(S) | -163923.54 | -40980.88 |
| 505 |  | SI3ZR5(S) | -609844.7 | -76230.59 |
| 506 |  | SI4ZR5(S) | -740504.31 | -82278.26 |
| 507 |  | SI511U489(S) | -51020979.51 | -51020.98 |
| 508 |  | SI5U3(S) | -419390.36 | -52423.8 |
| 509 |  | SR1(SER) | 0 | 0 |
| 510 |  | U1(SER) | 0 | 0 |
| 511 |  | ZR1(SER) | 0 | 0 |

Table 3 	Gaseous species stored in NUCLEA.

Gibbs energy at  T = 298.15 K

N°	SUBSTANCES                             	J / mole             J / g-atom

| 1 | AG1(G) | 233486.92 | 233486.92 |
| --- | --- | --- | --- |
| 2 | AG1O1(G) | 236080.35 | 118040.18 |
| 3 | AG2(G) | 330017.71 | 165008.86 |
| 4 | AL1(G) | 264978.9 | 264978.9 |
| 5 | AL1B1O2(G) | -621770.95 | -155442.74 |
| 6 | AL1C1(G) | 622924.02 | 311462.01 |
| 7 | AL1C2(G) | 610248.15 | 203416.05 |
| 8 | AL1H1(G) | 203428.25 | 101714.13 |
| 9 | AL1H1O1(G)1 | -30727.26 | -10242.42 |
| 10 | AL1H1O1(G)2 | -244386.47 | -81462.16 |
| 11 | AL1H1O2(G) | -536048.12 | -134012.03 |
| 12 | AL1H2(G) | 183524.24 | 61174.75 |
| 13 | AL1H2O2(G) | -727416.65 | -145483.33 |
| 14 | AL1H3(G) | 146618.21 | 36654.55 |
| 15 | AL1O1(G) | 12542.85 | 6271.42 |
| 16 | AL1O2(G) | -161240.88 | -53746.96 |
| 17 | AL2(G) | 417169.13 | 208584.57 |
| 18 | AL2C2(G) | 480147.51 | 120036.88 |
| 19 | AL2O1(G) | -261749.3 | -87249.77 |
| 20 | AL2O2(G) | -561018.6 | -140254.65 |
| 21 | AL2O3(G) | -643858.28 | -128771.66 |
| 22 | AR1(G) | -46156.01 | -46156.01 |
| 23 | B1(G) | 538182.95 | 538182.95 |
| 24 | B10H14(G) | -57690.78 | -2403.78 |
| 25 | B1BA1O2(G) | -721293.83 | -180323.46 |
| 26 | B1C1(G) | 766281.07 | 383140.53 |
| 27 | B1C2(G) | 720235.12 | 240078.37 |
| 28 | B1H1(G) | 391462.73 | 195731.36 |
| 29 | B1H1O1(G)1 | -258732.23 | -86244.08 |
| 30 | B1H1O1(G)2 | -84666.02 | -28222.01 |
| 31 | B1H1O2(G) | -632101.75 | -158025.44 |
| 32 | B1H2(G) | 147135.1 | 49045.03 |
| 33 | B1H2O1(G) | -138946.62 | -34736.66 |
| 34 | B1H2O2(G) | -549473.36 | -109894.67 |
| 35 | B1H3(G) | 50706.01 | 12676.5 |
| 36 | B1H3O1(G) | -358422.2 | -71684.44 |
| 37 | B1H3O2(G) | -720786.35 | -120131.06 |
| 38 | B1H3O3(G) | -1072202.07 | -153171.72 |
| 39 | B1O1(G) | -60631.53 | -30315.76 |
| 40 | B1O2(G) | -352997.53 | -117665.84 |
| 41 | B1O2SR1(G) | -716271.78 | -179067.94 |
| 42 | B2(G) | 792162.75 | 396081.38 |
| 43 | B2C1(G) | 712324.94 | 237441.65 |
| 44 | B2H4O4(G) | -1388487.46 | -138848.75 |
| 45 | B2H6(G) | -28491.53 | -3561.44 |
| 46 | B2O1(G) | 28362.76 | 9454.25 |
| 47 | B2O2(G) | -528356.26 | -132089.07 |
| 48 | B2O3(G) | -920534.72 | -184106.94 |
| 49 | B3H3O3(G) | -1304546.82 | -144949.65 |
| 50 | B3H3O6(G) | -2375509.78 | -197959.15 |
| 51 | B5H9(G) | -8866.58 | -633.33 |
| 52 | BA1(G) | 147398.23 | 147398.23 |
| 53 | BA1H1(G) | 138270.27 | 69135.14 |
| 54 | BA1H1O1(G) | -342305.72 | -114101.91 |
| 55 | BA1H2O2(G) | -719984.02 | -143996.8 |
| 56 | BA1O1(G) | -197909.36 | -98954.68 |
| 57 | BA2O1(G) | -327217.82 | -109072.61 |
| 58 | C1(G) | 669532.48 | 669532.48 |
| 59 | C1H1(G) | 539587.82 | 269793.91 |
| 60 | C1H1O1(G) | -23431.32 | -7810.44 |
| 61 | C1H1O2(G) | -288020.34 | -72005.08 |
| 62 | C1H2(G) | 328605.08 | 109535.03 |
| 63 | C1H2O1(G) | -181090.29 | -45272.57 |
| 64 | C1H2O2(G)C | -452963.2 | -90592.64 |
| 65 | C1H2O2(G)T | -436592.2 | -87318.44 |
| 66 | C1H3(G) | 87828.46 | 21957.11 |
| 67 | C1H3O1(G)1 | -56395.19 | -11279.04 |
| 68 | C1H3O1(G)2 | -93236.36 | -18647.27 |
| 69 | C1H4(G) | -130372.16 | -26074.43 |
| 70 | C1H4O1(G) | -272387.97 | -45397.99 |
| 71 | C1O1(G) | -169430.03 | -84715.01 |
| 72 | C1O2(G) | -457219.64 | -152406.55 |
| 73 | C1SI1(G) | 667555.34 | 333777.67 |
| 74 | C1SI2(G) | 484042.19 | 161347.4 |
| 75 | C1SI3(G) | 529657.73 | 132414.43 |
| 76 | C1SI4(G) | 551702.33 | 110340.47 |
| 77 | C2(G) | 778291.25 | 389145.63 |
| 78 | C2H1(G) | 415160.63 | 138386.88 |
| 79 | C2H2(G) | 166847.91 | 41711.98 |
| 80 | C2H2O1(G) | -119784.26 | -23956.85 |
| 81 | C2H2O2(G) | -293215.66 | -48869.28 |
| 82 | C2H3(G) | 190611.68 | 38122.34 |
| 83 | C2H4(G) | -12894.53 | -2149.09 |
| 84 | C2H4O1(G)1 | -125057.23 | -17865.32 |
| 85 | C2H4O1(G)2 | -244864.61 | -34980.66 |
| 86 | C2H4O2(G)1 | -516784.01 | -64598 |
| 87 | C2H4O2(G)2 | -439518.14 | -54939.77 |
| 88 | C2H4O4(G) | -920085.32 | -92008.53 |
| 89 | C2H5(G) | 34994.68 | 4999.24 |
| 90 | C2H6(G) | -153107.32 | -19138.41 |
| 91 | C2H6O1(G)1 | -318640.72 | -35404.52 |
| 92 | C2H6O1(G)2 | -263775.05 | -29308.34 |
| 93 | C2H6O1SI1(G) | -274911.06 | -27491.11 |
| 94 | C2H6O2(G) | -485787.25 | -48578.73 |
| 95 | C2H8SI1(G) | -161407.65 | -14673.42 |
| 96 | C2O1(G) | 217149.19 | 72383.06 |
| 97 | C2SI1(G) | 562356.42 | 187452.14 |
| 98 | C2SI2(G) | 565930.03 | 141482.51 |
| 99 | C2SI3(G) | 472155.08 | 94431.02 |
| 100 | C3(G) | 749329.1 | 249776.37 |
| 101 | C3H4(G)1 | 204503.03 | 29214.72 |
| 102 | C3H4(G)2 | 118253.14 | 16893.31 |
| 103 | C3H4(G)3 | 110450.99 | 15778.71 |
| 104 | C3H4O1(G)1 | -84410.12 | -10551.27 |
| 105 | C3H4O1(G)2 | -168823.64 | -21102.95 |
| 106 | C3H4O1(G)3 | -167782.93 | -20972.87 |
| 107 | C3H4O2(G)1 | -415216.78 | -46135.2 |
| 108 | C3H4O2(G)2 | -382412.32 | -42490.26 |
| 109 | C3H4O3(G) | -593676.05 | -59367.61 |
| 110 | C3H6(G)1 | -17441.99 | -1938 |
| 111 | C3H6(G)2 | -59792.92 | -6643.66 |
| 112 | C3H6O1(G)1 | -223601.81 | -22360.18 |
| 113 | C3H6O1(G)2 | -177491.66 | -17749.17 |
| 114 | C3H6O1(G)3 | -305159.22 | -30515.92 |
| 115 | C3H6O1(G)4 | -276757.48 | -27675.75 |
| 116 | C3H6O1(G)5 | -221370.51 | -22137.05 |
| 117 | C3H6O2(G) | -508581.67 | -46234.7 |
| 118 | C3H6O3(G) | -551960.79 | -45996.73 |
| 119 | C3H7(G)1 | -9699.87 | -969.99 |
| 120 | C3H7(G)2 | 1058.53 | 105.85 |
| 121 | C3H8(G) | -184320.5 | -16756.41 |
| 122 | C3H8O1(G)1 | -308670.85 | -25722.57 |
| 123 | C3H8O1(G)2 | -351344.01 | -29278.67 |
| 124 | C3H8O1(G)3 | -364855.88 | -30404.66 |
| 125 | C3O2(G) | -175919.11 | -35183.82 |
| 126 | C4(G) | 902613.79 | 225653.45 |
| 127 | C4NI1O4(G) | -722670.52 | -80296.72 |
| 128 | C5(G) | 906912.04 | 181382.41 |
| 129 | C5FE1O5(G) | -858789.13 | -78071.74 |
| 130 | C6CR1O6(G) | -1151001.24 | -88538.56 |
| 131 | CA1(G) | 131470.25 | 131470.25 |
| 132 | CA1H1(G) | 168749.71 | 84374.85 |
| 133 | CA1H1O1(G) | -264083.57 | -88027.86 |
| 134 | CA1H2O2(G) | -695884.08 | -139176.82 |
| 135 | CA1O1(G) | -21543.41 | -10771.71 |
| 136 | CA2(G) | 260561.61 | 130280.81 |
| 137 | CR1(G) | 364370.65 | 364370.65 |
| 138 | CR1O1(G) | 116976.46 | 58488.23 |
| 139 | CR1O2(G) | -155552.34 | -51850.78 |
| 140 | CR1O3(G) | -372207.2 | -93051.8 |
| 141 | CR2(G) | 558217.14 | 279108.57 |
| 142 | FE1(G) | 357670.39 | 357670.39 |
| 143 | FE1H2O2(G) | -414938.69 | -82987.74 |
| 144 | FE1O1(G) | 178944.32 | 89472.16 |
| 145 | FE2(G) | 469463.25 | 234731.63 |
| 146 | H1(G) | 183796.42 | 183796.42 |
| 147 | H1IN1(G) | 152854.46 | 76427.23 |
| 148 | H1IN1O1(G) | -177715.11 | -59238.37 |
| 149 | H1MG1(G) | 111463.34 | 55731.67 |
| 150 | H1MG1O1(G) | -239351.24 | -79783.75 |
| 151 | H1NI1(G) | 330523.83 | 165261.92 |
| 152 | H1O1(G) | -15399.56 | -7699.78 |
| 153 | H1O1SR1(G) | -264116.81 | -88038.94 |
| 154 | H1O2(G) | -65748.6 | -21916.2 |
| 155 | H1SI1(G) | 317547.68 | 158773.84 |
| 156 | H1SR1(G) | 155860.43 | 77930.22 |
| 157 | H1ZR1(G) | 451889.28 | 225944.64 |
| 158 | H2(G) | -38929.31 | -19464.66 |
| 159 | H2MG1O2(G) | -651873.04 | -130374.61 |
| 160 | H2NI1O2(G) | -342047.19 | -68409.44 |
| 161 | H2O1(G) | -298082.19 | -99360.73 |
| 162 | H2O2(G) | -205539.12 | -51384.78 |
| 163 | H2O2SR1(G) | -673915.64 | -134783.13 |
| 164 | H2SI1(G) | 211505.15 | 70501.72 |
| 165 | H3SI1(G) | 139897.6 | 34974.4 |
| 166 | H4SI1(G) | -26675.76 | -5335.15 |
| 167 | H6SI2(G) | -960.95 | -120.12 |
| 168 | IN1(G) | 188905.56 | 188905.56 |
| 169 | IN1O1(G) | 99366.94 | 49683.47 |
| 170 | IN2(G) | 317670.57 | 158835.28 |
| 171 | IN2O1(G) | -132009.52 | -44003.17 |
| 172 | LA1(G) | 361792.21 | 361792.21 |
| 173 | LA1O1(G) | -192451.31 | -96225.65 |
| 174 | LA2O1(G) | -141915.24 | -47305.08 |
| 175 | LA2O2(G) | -715506.87 | -178876.72 |
| 176 | MG1(G) | 99565.8 | 99565.8 |
| 177 | MG1O1(G) | -5395.48 | -2697.74 |
| 178 | MG2(G) | 203668.81 | 101834.4 |
| 179 | NI1(G) | 367484.91 | 367484.91 |
| 180 | NI1O1(G) | 237687.74 | 118843.87 |
| 181 | O1(G) | 201160.56 | 201160.56 |
| 182 | O1SI1(G) | -159349.18 | -79674.59 |
| 183 | O1SR1(G) | -70257.88 | -35128.94 |
| 184 | O1U1(G) | -45138.27 | -22569.14 |
| 185 | O1ZR1(G) | 14500.96 | 7250.48 |
| 186 | O2(G) | -61164.58 | -30582.29 |
| 187 | O2SI1(G) | -373666.79 | -124555.6 |
| 188 | O2SI2(G) | -490058.61 | -122514.65 |
| 189 | O2U1(G) | -553546.13 | -184515.38 |
| 190 | O2ZR1(G) | -477564.43 | -159188.14 |
| 191 | O3(G) | 70540.6 | 23513.53 |
| 192 | O3RU1(G) | -160573.12 | -40143.28 |
| 193 | O3U1(G) | -897302.47 | -224325.62 |
| 194 | O4RU1(G) | -269585.7 | -53917.14 |
| 195 | RU1(G) | 600987.7 | 600987.7 |
| 196 | SI1(G) | 400042.8 | 400042.8 |
| 197 | SI2(G) | 511590.2 | 255795.1 |
| 198 | SI3(G) | 542661.22 | 180887.07 |
| 199 | SR1(G) | 111785.53 | 111785.53 |
| 200 | SR2(G) | 228192.96 | 114096.48 |
| 201 | U1(G) | 476549.41 | 476549.41 |
| 202 | ZR1(G) | 535132.84 | 535132.84 |
| 203 | ZR2(G) | 851510.77 | 425755.38 |

3.	STATE of VALIDATION

The state of validation of a thermodynamic database is characterised by the good agreement between calculated and available experimental results (phase diagrams and thermodynamic properties) concerning basic sub-systems (binary, ternary, …) or practical global experiments, made in similar conditions and at thermodynamic equilibrium.

For user information, a quality criterion, based on comparison between calculation and available experimental data, has been established for each assessed sub-system.

 	Estimated

No experimental data available.

	Perfectible

Some domains need more experimental information (phase diagram or thermodynamic properties).

	Acceptable

The system is well known and satisfactorily modelled.

	High quality

The system is quite known and modelled.

The complete list of the 153 (18*17/2) metal-metal or metal-oxygen binary systems based on pure elements and 105 (15*14/2) oxide pseudo-binary systems based on pure oxides are presented in tables 5 and 6 respectively.

Due to the very high number of possible ternary (18*17*16/3*2 = 816) and pseudo-ternary (15*14*13/3*2 = 455) systems, it is completely unimaginable to assess all of them in a human delay. For that reason it was decided to assess only the most important ternary systems for practical applications. The list of the selected ternary and pseudo-ternary systems is presented in tables 7 and 8 respectively.

For each system, the order number, source and provisional quality criterion are given. This criterion takes into account both phase diagram and thermodynamic properties, and thus cannot be indicated only on a phase diagram. This point is fundamental for the modelling of multi-component systems.

Moreover, it must be kept in mind that the set of a quality criterion remains somewhere subjective, and the improvement of existing sub-systems with newly available experimental results is a continuous task, which is part of the database management and updating.

# 3.1.	BINARY AND PSEUDO-BINARY SYSTEMS.

Table 4	Binary systems.

| System | Quality | Date of issue |  | System | Quality | Date of issue |  | System | Quality | Date of issue |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ag-Al |  | 03/2003 |  | Ba-Fe |  | 03/2003 |  | Fe-O |  | 03/2003 |
| Ag-B |  | 01/2006 |  | Ba-In |  | 03/2003 |  | Fe-Ru |  | 03/2003 |
| Ag-Ba |  | 03/2003 |  | Ba-La |  | 03/2003 |  | Fe-Si |  | 03/2003 |
| Ag-C |  | 01/2006 |  | Ba-Mg |  | 03/2003 |  | Fe-Sr |  | 03/2003 |
| Ag-Ca |  | 03/2003 |  | Ba-Ni |  | 03/2003 |  | Fe-U |  | 01/2005 |
| Ag-Cr |  | 03/2003 |  | Ba-O |  | 03/2003 |  | Fe-Zr |  | 01/2005 |
| Ag-Fe |  | 03/2003 |  | Ba-Ru |  | 03/2003 |  | In-La |  | 03/2003 |
| Ag-In |  | 03/2003 |  | Ba-Si |  | 03/2003 |  | In-Mg |  | 03/2003 |
| Ag-La |  | 03/2003 |  | Ba-Sr |  | 03/2003 |  | In-Ni |  | 03/2003 |
| Ag-Mg |  | 03/2003 |  | Ba-U |  | 03/2003 |  | In-O |  | 03/2003 |
| Ag-Ni |  | 03/2003 |  | Ba-Zr |  | 03/2003 |  | In-Ru |  | 03/2003 |
| Ag-O |  | 03/2003 |  | C-Ca |  | 01/2006 |  | In-Si |  | 03/2003 |
| Ag-Ru |  | 03/2003 |  | C-Cr |  | 03/2003 |  | In-Sr |  | 03/2003 |
| Ag-Si |  | 03/2003 |  | C-Fe |  | 03/2003 |  | In-U |  | 03/2003 |
| Ag-Sr |  | 03/2003 |  | C-In |  | 03/2003 |  | In-Zr |  | 03/2003 |
| Ag-U |  | 03/2003 |  | C-La |  | 03/2003 |  | La-Mg |  | 03/2003 |
| Ag-Zr |  | 03/2003 |  | C-Mg |  | 01/2006 |  | La-Ni |  | 03/2003 |
| Al-B |  | 03/2003 |  | C-Ni |  | 03/2003 |  | La-O |  | 03/2003 |
| Al-Ba |  | 03/2003 |  | C-O |  | 03/2003 |  | La-Ru |  | 01/2006 |
| Al-C |  | 03/2003 |  | C-Ru |  | 03/2003 |  | La-Si |  | 03/2003 |
| Al-Ca |  | 03/2003 |  | C-Si |  | 03/2003 |  | La-Sr |  | 03/2003 |
| Al-Cr |  | 01/2006 |  | C-Sr |  | 01/2006 |  | La-U |  | 03/2003 |
| Al-Fe |  | 03/2003 |  | C-U |  | 03/2003 |  | La-Zr |  | 03/2003 |
| Al-In |  | 03/2003 |  | C-Zr |  | 03/2003 |  | Mg-Ni |  | 03/2003 |
| Al-La |  | 03/2003 |  | Ca-Cr |  | 03/2003 |  | Mg-O |  | 03/2003 |
| Al-Mg |  | 03/2003 |  | Ca-Fe |  | 03/2003 |  | Mg-Ru |  | 03/2003 |
| Al-Ni |  | 03/2003 |  | Ca-In |  | 03/2003 |  | Mg-Si |  | 03/2003 |
| Al-O |  | 03/2003 |  | Ca-La |  | 03/2003 |  | Mg-Sr |  | 03/2003 |
| Al-Ru |  | 03/2003 |  | Ca-Mg |  | 01/2006 |  | Mg-U |  | 03/2003 |
| Al-Si |  | 03/2003 |  | Ca-Ni |  | 03/2003 |  | Mg-Zr |  | 03/2003 |
| Al-Sr |  | 03/2003 |  | Ca-O |  | 03/2003 |  | Ni-O |  | 03/2003 |
| Al-U |  | 03/2003 |  | Ca-Ru |  | 03/2003 |  | Ni-Ru |  | 03/2003 |
| Al-Zr |  | 03/2003 |  | Ca-Si |  | 03/2003 |  | Ni-Si |  | 01/2006 |
| B-Ba |  | 03/2003 |  | Ca-Sr |  | 03/2003 |  | Ni-Sr |  | 03/2003 |
| B-C |  | 03/2003 |  | Ca-U |  | 03/2003 |  | Ni-U |  | 03/2003 |
| B-Ca |  | 03/2003 |  | Ca-Zr |  | 03/2003 |  | Ni-Zr |  | 03/2003 |
| B-Cr |  | 03/2003 |  | Cr-Fe |  | 03/2003 |  | O-Ru |  | 03/2003 |
| B-Fe |  | 03/2003 |  | Cr-In |  | 03/2003 |  | O-Si |  | 03/2003 |
| B-In |  | 03/2003 |  | Cr-La |  | 03/2003 |  | O-Sr |  | 03/2003 |
| B-La |  | 03/2003 |  | Cr-Mg |  | 03/2003 |  | O-U |  | 01/2006 |
| B-Mg |  | 03/2003 |  | Cr-Ni |  | 03/2003 |  | O-Zr |  | 01/2005 |
| B-Ni |  | 03/2003 |  | Cr-O |  | 03/2003 |  | Ru-Si |  | 03/2003 |
| B-O |  | 03/2003 |  | Cr-Ru |  | 03/2003 |  | Ru-Sr |  | 03/2003 |
| B-Ru |  | 01/2006 |  | Cr-Si |  | 03/2003 |  | Ru-U |  | 01/2006 |
| B-Si |  | 03/2003 |  | Cr-Sr |  | 03/2003 |  | Ru-Zr |  | 03/2003 |
| B-Sr |  | 03/2003 |  | Cr-U |  | 03/2003 |  | Si-Sr |  | 03/2003 |
| B-U |  | 03/2003 |  | Cr-Zr |  | 03/2003 |  | Si-U |  | 03/2003 |
| B-Zr |  | 03/2003 |  | Fe-In |  | 03/2003 |  | Si-Zr |  | 03/2003 |
| Ba-C |  | 03/2003 |  | Fe-La |  | 03/2003 |  | Sr-U |  | 03/2003 |
| Ba-Ca |  | 03/2003 |  | Fe-Mg |  | 03/2003 |  | Sr-Zr |  | 03/2003 |
| Ba-Cr |  | 03/2003 |  | Fe-Ni |  | 03/2003 |  | U-Zr |  | 01/2005 |

Table 5	Pseudo-binary systems.

| System | Quality | Date of issue |  | System | Quality | Date of issue |  | System | Quality | Date of issue |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al2O3-B2O3 |  | 03/2003 |  | BaO-O2U |  | 03/2003 |  | Fe2O3-O2Si |  | 03/2003 |
| Al2O3-BaO |  | 03/2003 |  | BaO-O2Zr |  | 03/2003 |  | Fe2O3-O2U |  | 03/2003 |
| Al2O3-CaO |  | 01/2006 |  | CaO-Cr2O3 |  | 03/2003 |  | Fe2O3-O2Zr |  | 03/2003 |
| Al2O3-Cr2O3 |  | 03/2003 |  | CaO-FeO |  | 03/2003 |  | In2O3-La2O3 |  | 03/2003 |
| Al2O3-FeO |  | 03/2003 |  | CaO-Fe2O3 |  | 03/2003 |  | In2O3-MgO |  | 03/2003 |
| Al2O3-Fe2O3 |  | 03/2003 |  | CaO-In2O3 |  | 03/2003 |  | In2O3-NiO |  | 03/2003 |
| Al2O3-In2O3 |  | 03/2003 |  | CaO-La2O3 |  | 03/2003 |  | In2O3-OSr |  | 03/2003 |
| Al2O3-La2O3 |  | 03/2003 |  | CaO-MgO |  | 03/2003 |  | In2O3-O2Si |  | 03/2003 |
| Al2O3-MgO |  | 03/2003 |  | CaO-NiO |  | 03/2003 |  | In2O3-O2U |  | 03/2003 |
| Al2O3-NiO |  | 03/2003 |  | CaO-OSr |  | 03/2003 |  | In2O3-O2Zr |  | 03/2003 |
| Al2O3-OSr |  | 03/2003 |  | CaO-O2Si |  | 03/2003 |  | La2O3-MgO |  | 03/2003 |
| Al2O3-O2Si |  | 03/2003 |  | CaO-O2U |  | 03/2003 |  | La2O3-NiO |  | 03/2003 |
| Al2O3-O2U |  | 03/2003 |  | CaO-O2Zr |  | 03/2003 |  | La2O3-OSr |  | 03/2003 |
| Al2O3-O2Zr |  | 03/2003 |  | Cr2O3-FeO |  | 03/2003 |  | La2O3-O2Si |  | 03/2003 |
| B2O3-BaO |  | 03/2003 |  | Cr2O3-Fe2O3 |  | 12/2004 |  | La2O3-O2U |  | 03/2003 |
| B2O3-CaO |  | 03/2003 |  | Cr2O3-In2O3 |  | 03/2003 |  | La2O3-O2Zr |  | 03/2003 |
| B2O3-Cr2O3 |  | 03/2003 |  | Cr2O3-La2O3 |  | 03/2003 |  | MgO-NiO |  | 03/2003 |
| B2O3-FeO |  | 03/2003 |  | Cr2O3-MgO |  | 03/2003 |  | MgO-OSr |  | 03/2003 |
| B2O3-Fe2O3 |  | 03/2003 |  | Cr2O3-NiO |  | 12/2004 |  | MgO-O2Si |  | 03/2003 |
| B2O3-In2O3 |  | 03/2003 |  | Cr2O3-OSr |  | 03/2003 |  | MgO-O2U |  | 03/2003 |
| B2O3-La2O3 |  | 03/2003 |  | Cr2O3-O2Si |  | 03/2003 |  | MgO-O2Zr |  | 03/2003 |
| B2O3-MgO |  | 03/2003 |  | Cr2O3-O2U |  | 03/2003 |  | NiO-OSr |  | 03/2003 |
| B2O3-NiO |  | 03/2003 |  | Cr2O3-O2Zr |  | 03/2003 |  | NiO-O2Si |  | 03/2003 |
| B2O3-OSr |  | 03/2003 |  | FeO-Fe2O3 |  | 03/2003 |  | NiO-O2U |  | 03/2003 |
| B2O3-O2Si |  | 03/2003 |  | FeO-In2O3 |  | 03/2003 |  | NiO-O2Zr |  | 03/2003 |
| B2O3-O2U |  | 03/2003 |  | FeO-La2O3 |  | 03/2003 |  | OSr-O2Si |  | 03/2003 |
| B2O3-O2Zr |  | 03/2003 |  | FeO-MgO |  | 03/2003 |  | OSr-O2U |  | 03/2003 |
| BaO-CaO |  | 03/2003 |  | FeO-NiO |  | 03/2003 |  | OSr-O2Zr |  | 03/2003 |
| BaO-Cr2O3 |  | 03/2003 |  | FeO-OSr |  | 03/2003 |  | O2Si-O2U |  | 03/2003 |
| BaO-FeO |  | 03/2003 |  | FeO-O2Si |  | 03/2003 |  | O2Si-O2Zr |  | 03/2003 |
| BaO-Fe2O3 |  | 03/2003 |  | FeO-O2U |  | 03/2003 |  | O2U-O2Zr |  | 01/2005 |
| BaO-In2O3 |  | 03/2003 |  | FeO-O2Zr |  | 03/2003 |  |  |  |  |
| BaO-La2O3 |  | 03/2003 |  | Fe2O3-In2O3 |  | 03/2003 |  |  |  |  |
| BaO-MgO |  | 03/2003 |  | Fe2O3-La2O3 |  | 03/2003 |  |  |  |  |
| BaO-NiO |  | 03/2003 |  | Fe2O3-MgO |  | 03/2003 |  |  |  |  |
| BaO-OSr |  | 03/2003 |  | Fe2O3-NiO |  | 03/2003 |  |  |  |  |
| BaO-O2Si |  | 03/2003 |  | Fe2O3-OSr |  | 03/2003 |  |  |  |  |

3.2.	SELECTED TERNARY AND PSEUDO-TERNARY SYSTEMS.

Table 6	Ternary systems.

| System | Quality | Date of issue |  | System | Quality | Date of issue |  | System | Quality | Date of issue |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| B-C-Fe |  | 03/2003 |  | C-Fe-Ni |  | 03/2003 |  | Cr-Fe-Zr |  | 03/2003 |
| B-C-U |  | 03/2003 |  | C-O-U |  | 03/2003 |  | Cr-Ni-O |  | 03/2003 |
| B-C-Zr |  | 03/2003 |  | C-O-Zr |  | 03/2003 |  | Fe-Ni-O |  | 03/2003 |
| B-Fe-U |  | 03/2003 |  | C-U-Zr |  | 03/2003 |  | Fe-O-Si |  | 01/2006 |
| B-Fe-Zr |  | 03/2003 |  | Ca-Fe-O |  | 01/2006 |  | Fe-O-U |  | 01/2005 |
| C-Cr-Fe |  | 03/2003 |  | Cr-Fe-Ni |  | 03/2003 |  | Fe-O-Zr |  | 01/2005 |
| C-Cr-Ni |  | 03/2003 |  | Cr-Fe-O |  | 03/2003 |  | Fe-U-Zr |  | 01/2005 |
|  |  |  |  |  |  |  |  | O-U-Zr |  | 01/2006 |

Table 7	Pseudo-ternary systems.

| System | Quality | Date of issue |  | System | Quality | Date of issue |
| --- | --- | --- | --- | --- | --- | --- |
| Al2O3-B2O3-CaO |  | 03/2003 |  | Al2O3-O2U-O2Zr |  | 03/2003 |
| Al2O3-B2O3-O2Si |  | 03/2003 |  | B2O3-CaO-MgO |  | 03/2003 |
| Al2O3-B2O3-MgO |  | 03/2003 |  | B2O3-CaO-O2Si |  | 03/2003 |
| Al2O3-CaO-O2Si |  | 03/2003 |  | B2O3-FeO-Fe2O3 |  | 03/2003 |
| Al2O3-O2Si-O2U |  | 03/2003 |  | B2O3-MgO-O2Si |  | 03/2003 |
| Al2O3-O2Si-O2Zr |  | 03/2003 |  | O2Si-O2U-O2Zr |  | 03/2003 |

3.3.	DOMAIN OF APPLICATION AND LIMITATIONS.

In this version of NUCLEA most of the binary and pseudo-binary systems have been analysed and critically assessed either by THERMODATA or AEA-T.

Only a limited number of binary systems (mainly based on the C-Cr-Fe-Ni quaternary system) were taken in open literature.

However, some of them are still insufficiently known, and further experimental work is needed for the ones interesting the nuclear field.

In a very high-number component system such as the one covered by NUCLEA, the number of possible ternaries and pseudo-ternaries is equal to 1271, while the time cost to assess only one is about one-man year. Few experimental data are available in open literature for ternaries of high interest for nuclear safety. Consequently, the complete assessment of all ternaries is not achievable in a human delay and only some selected ternary systems of main importance for nuclear safety applications were assessed at this time.

Moreover, a simple overlook of the stars attributed to all sub-systems is not the best approach to estimate the global quality of the database. In fact, only some sub-systems are especially relevant in the nuclear domain. The quality of these specific sub-systems, designated by principal users, is much more important for NUCLEA dedicated to severe accident applications. Thus, further work will still have to be done for the selected sub-systems with less than three stars.

In any case, well-selected global experiments will always have to be done to validate definitively the thermodynamic approach on the final user point of view.

Simultaneously, fulfilling and improving the sub-systems in the NUCLEA is a continuous task, the assessment work being based on the CALPHAD method, and ideally never completely realised.

In summary, the Nuclear Thermodynamic Database could be considered as well validated if sufficient predicting power was reached for practical applications, both in the In- and Ex-Vessel fields.

3.4.	FUTURE.

In the future, specific actions will have to be foreseen to improve the state of validation of NUCLEA, both for In- and Ex- Vessel applications.

- On the one hand, such a database must be continuously updated for all binary or pseudo-binary, and selected ternary sub-systems, by taking into account the newly available experimental results in the optimisation process based on the CALPHAD method.

- On the other hand, the database must also be compared to available experimental results in higher-order systems, in order to validate the global thermodynamic approach or eventually to identify remaining uncertainties or insufficient knowledge.

This task involves two different aspects :

- Obviously a very high quality scientific work for obtaining reliable thermodynamic data, by using adapted thermodynamic models and sophisticated optimisation codes.

- But also a considerable technical work, which is the database management, in order to maintain an updated experimental database (phase diagram and thermodynamic properties), and to be able to re-assess binary or ternary sub-systems if necessary, when new experiments becomes available.

4.	ASSESSMENT of FE-O-U-ZR

An important experimental and modelisation work was done in the last 10 years by many people in the world to obtain now a rather good knowledge and representation of that main quaternary system.

In the present version of the database all the available information (equilibrium points of phase diagrams, activities measurements, vapour pressures etc…), up to the year 2004, was taken into account in the optimisation procedure.

To allow the user to have an idea of the validity of the obtained results the calculated phase diagrams are compared, in the following pages, with some experimental points. But if anybody is interested more in detail by the experiments or by critical assessment and optimisation work he has to look at the numerous scientific papers published in the recent years.

4.1.	BINARY SYSTEMS.

Fe-O, Fe-U, Fe-Zr, O-U, O-Zr, U,Zr.

# 4.2.	PSEUDO-BINARY SYSTEMS.

O2U-O2Zr.

IMPORTANT NOTE :

It must be underlined that pseudo-binary systems including iron oxides are not real quasi-binary phase diagrams. These ones are only used for evaluation of the interaction parameters, but they have to be further controlled by calculating them as valid sections of the ternary systems Fe-O-U or Fe-O-Zr.

4.3.	TERNARY SYSTEMS.

Fe-O-U, Fe-O-Zr, Fe-U-Zr, O-U-Zr.

FE-O

The phase diagram of the Fe-O binary system presents the following condensed solutions and substances, with the symbols used in this work or found in open literature :

- the liquid phase, L, which shows a miscibility gap between an Fe rich liquid (L1) and an FeO/Fe2O3 rich liquid (L2) ;

- the intermediate solid oxides, Fe3O4(S) or magnetite, Fe2O3(S) or hematite, corundum ;

- the oxide solid solution, FeO1+x, or wustite, with the face-centred cubic structure, of NaCl type, noted fcc_B1 ;

- pure solid iron, with a negligible solubility of oxygen, and different allotropic structures, cubic face centred (fcc_A1) and body cubic centred (bcc_A2) ;

- the gas phase, which shows an extended solubility of iron in oxygen above 2800 K.

The fundamental thermodynamic properties (Cp, H298, S298) of the stoichiometric compounds Fe0.947O1(fcc_B1), Fe3O4(S), Fe2O3(S) have been assessed separately in consistency with the available experimental data.  The liquid phase has been described by a non-ideal associate model, with the formula (Fe1, Fe1 O1, Fe1O1.5,O1)(L), and the solid solution  FeO1+x  by a simple one lattice model, with the formula (Fe1O1, Fe1O1.5)(fcc_B1). The gas phase has been described by an ideal mixture of gaseous species, with the formula (Fe1, Fe1O1, Fe1O1.5, O1, O2, O3)1(G).

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- the activity of iron and oxygen are in satisfactory agreement with the experimental ones in the solid state and are strongly constrained by the assessed thermodynamic properties of stoichiometric compounds ;

- the wustite phase limits are very well reproduced ;

- the liquidus in the iron rich region is in satisfactory agreement with the experimental one up to 2200 K, as well as the melting point of Fe3O4(S) and all the invariant reactions ;

- the miscibility gap in the liquid state was assumed to be closed around 3000 K, in agreement with only one series of experimental points, which should be validated again.

Figure 1	Calculated Fe-O phase diagram with special points and invariant reactions.

Figure 2	Calculated Fe-O phase diagram compared with selected experimental data.

[1929Sch]	"Equilibrium investigations on the reduction, oxidation and carburization processes in iron. VIII"

R. Schenck, T. Dingmann, P.H. Kirscht and H. Wesselkock,

Z. Anorg. Allg. Chem., 182, 97-117 (1929).

[1931Pfe]	"The constitution of scale"

L.B. Pfeil,

J. Iron Steel Inst., 123, 237-255 (1931).

[1933Jet]	 "A study of the homogeneity limits of wüstite (FeO) by X-Ray methods"

E.R. Jette and F. Foote,

Trans. AIME, 105, 276-284 (1933).

[1941Chi]	" "

J. Chipman and K.L. Fetters,

Trans. ASM, 29, 953-967 (1941).

[1943Tay]	" "

C.R. Taylor and J. Chipman,

Trans. AIME, 154, 228-245 (1943).

[1945Dar]	"The system iron-oxygen. I. The wüstite field and related equilibria"

L.S. Darken and R.W. Gurry,

J. Am. Chem. Soc., 67, 1398-1412 (1945).

[1949Ben]	"Research on variations in composition of wüstite"

J. Benard,

Bull. Soc. Chim. Fr. (Ser.5), 16, D109-D119 (1949).

[1949San]	"Reduction equilibria of iron oxides. I. Measurement of the equilibrium of reaction Fe3O4 (in wüstite) + CO = 3 FeO (in wüstite) + CO2"

K. Sanbongi,

Sci. Rep. Res. Inst. Tohoku Univ., 1 , 213-222 (1949).

[1951Cir]	"The limits of composition of wüstite"

V. Cirilli and C. Brisi,

Ann. Chimica, 41, 508-514 (1951).

[1954Ari]	"Thermodynamics of oxide phases with variable compositions. I. Thermodynamics of iron protoxide"

S.M. Ariya, M.P. Mororozova and L.A. Shneider,

Zh. Obshch. Khim., 24, 41-47 (1954).

[1955Mar]	"Contribution to the study of iron protoxide"

F. Marion,

Doc. Metall., (Soc. Ind. Miner. St Etienne), Paris, 24, 87-136, (1955).

[1956Gok]	"Equilibria in reaction of hydrogen, and carbon monoxide with dissolved oxygen in liquid iron ; equilibrium in reduction of ferrous oxide with hydrogen, and solubility of oxygen in liquid iron"

N.A. Gokcen,

Trans. AIME, 206, 1558-1567 (1956).

[1956Hov]	"The oxygen content of wüstite in equilibrium with different gases"

N.A. Hovgard and P.N. Jensfelt,

Jernkontorets Ann., 140, 467-493 (1956).

[1958Sve]	" "

V.N. Svechnikov, V.M. Pan and A.K. Shurin,

Fiz. Metal. i Metalloved, 6, 662-664 (1958) ; Phys. Metals Metallog. (USSR), 6, 4, 80-82 (1958).

[1961Sch]	" "

H.Schenck und W.Pfaff,

Archiv fuer Eisenhuttenwesen, Vol. 32, 741-751, (1961).

[1963Off]	"Contribution to the study of iron protoxide. I. Limits of the iron protoxide phase"

C. Offroy and J. Aubry,

Mem. Sci. Rev. Metall., 60, 6, 476-480 (1963).

Figure 3	Calculated Fe-O phase diagram compared with selected experimental data.

[1964Bar]	"The stability of wüstite by electromotive force measurements on all-solid electrolytic cells"

G.B. Barbi,

J. Phys. Chem., 68, 10, 2912-2916 (1964).

[1964Ger]	"Utilization of the thermobalance in experiments on transfer of oxygen between oxides"

P. Gerdanian and M. Dode,

C.R. Acad. Sci. (Paris), 258, 892-895 (1964).

[1965Meu]	"Studies of high-temperature materials (properties of FeO)"

R.A. Meussner, L.E. Richards and C.T. Fujii,

Rep. NRL Prog. Naval Res. Lab. Washington, DC, 26-28 (1965). Cited by          [1968Riz2].

[1966Ack]	"A thermodynamic study of the wüstite phase"

R.J. Ackermann and R.W. Sandford Jr.,

USAEC, Argonne Nat. Lab., Rep. ANL-7250 (1966).

[1967Bel]	"Determination of the solubility of oxygen in molten iron, cobalt and nickel"

B.F. Belov, I.A. Novokhatskiy and Yu.A. Lobanov,

Izv. Akad. Nauk SSSR, Met., 3, 53-62 (1967) ; Russ. Metall., 3, 19-23, (1967).

[1967Swa]	"On the vacancy concentration of wüstite (FeOx) near the p to n transition"

B. Swaroop and J.B. Wagner, Jr.,

Trans. Metall. Soc. AIME, 239, 1215-1218 (1967).

[1968Fuj]	"Chromium solubility in wüstite at 1000°C : changes in oxygen activity and lattice parameter"

C.T. Fujii and R.A. Meussner,

Trans. Metall. Soc. AIME, 242, 1259-1265 (1968).

[1968Riz]	"Coulometric titration of wüstite"

F.E. Rizzo and J.V. Smith,

J. Phys. Chem., 72, 2, 485-488 (1968).

[1969Cam]	"Determination of the boundaries of the iron protoxyde domain at high temperature"

J. Campserveux, G. Boureau, C. Picard and P. Gerdanian,

Rev. Int. Hautes Temp. Refract., 6, 165-174 (1969).

[1969Lyk]	"Thermodynamics of wüstite"

A.A. Lykasov, Yu.S. Kuznetsov, E.I. Pil'Ko, V.I. Shishkov and V.A. Kozheurov,

Zh. Fiz. Khim., 43, 12, 3124-3125 (1969).

[1969Riz]	"The determination of phase boundaries and thermodynamic functions in the iron-oxygen system by EMF measurements"

H.F. Rizzo, R.S. Gordon and I.B. Cutler,

J. Electochem. Soc., 116, 2, 266-274 (1969).

[1970Asa]	"Thermodynamic properties of wüstite(FeO(1+y))"

H. Asao, K. Ono, A. Yamaguchi and J. Moriyama,

Mem. Fac. Eng., Kyoto Univ., 33, 66-77 (1970).

[1970Cir]	"Limits of composition of wüstite and solid solutions among wüstite, calcium oxide, and magnesium oxide"

V. Cirilli, A. Burdese and C. Brisi,

Ann. Chim. (Paris), 5, 4, 283-286 (1970).

[1970Mar]	"Determination of partial molar magnitudes of mixing of oxygen in iron protoxide at 1075°C. II. Measurements of s(O2)M"

J.F. Marucco, C. Picard, P. Gerdanian and D. Dode,

J. Chim. Phys. Phys.-Chim. Biol., 67, 914-916 (1970).

Figure 4	Calculated Fe-O phase diagram compared with selected experimental data.

[1971Dis]	"Solubility of oxygen in liquid iron from 1785 to 1960°C. A new technique for the study of slag metal equilibria"

P.A. Distin, S.G. Whiteway and C.R. Mason,

Can. Metall. Q., 10, 1, 13-18 (1971).

[1974Gid]	"Solid-state coulometric titration: critical analysis and application to wustite"

R.A. Giddings and R.S. Gordon,

J. Electrochem. Soc., 121, 6, 793-800 (1974).

[1978Fis]	"The solubility of oxygen in pure iron from the melting point to 2046°C, determined with the levitation melting method"

W.A. Fischer and J.F. Schumacher,

Arch. Eisenhüttenwes., 49, 9, 431-435 (1978).

[1980Tak]	"Thermodynamic properties and subphases of wustite field determined by means of thermogravimetric method in the temperature range of 1100-1300°C"

E. Takayama and N. Kimizukaon,

J. Electrochem. Soc., 127, 4, 970-976 (1980).

[1981Bar]	"The lower temperature range of the wustite stability field"

J.A. Barbero, M.A. Blesa and J.G. Moroto,

Z. Phys. Chem. Neue Folge, 124, 139-147 (1981).

[1983Ndu]	"The solubility of liquid oxysulfide phase in liquid Fe-O-S alloys"

M. Nduaguba and J.F. Elliott,

Metall. Trans. B, 14, 679-683 (1983).

[1989Val]	"The Fe-O (Iron-Oxygen) phase diagram in the range of the non-stoichiometric monoxide and magnetite at the Fe-rich limit : reduction diagrams"

P. Vallet,

Bull. Alloy Phase Diagrams, 10, 3,  209-218 (1989).

[1991Wri]	"The Fe-O (Iron-Oxygen) system"

H.A. Wriedt,

J. Phase Equilibria, 12, 2, 170-200 (1991).

[1984Oth]	"Composition of the core : I. solubility of oxygen in molten iron at high temperatures"

E. Ohtani and A.E. Ringwood,

Earth Plan. Sci. Lett., 71, 85-93 (1984).

FE-U

The phase diagram of the Fe-U binary system presents the following condensed solutions and substances, with the symbols used in this work or found in open literature :

- the liquid phase, L, which shows a complete miscibility from iron to uranium ;

- the intermetallic compounds, Fe2U1(S) with the Laves structure, and Fe1U6(S) ;

- pure solid iron, with a negligible solubility of uranium, with two allotropic structures, Fe1(bcc_A2) and Fe1(fcc_A1) ;

- the uranium rich terminal solid solutions, tetragonal (tet) and body cubic centred, bcc_A2, with a small solubility of iron.

- pure orthorhombic uranium U1(ort_A20),  with a negligible solubility of iron.

The heat capacity (Cp) of the stoichiometric compounds Fe2U1(S) and Fe1U6(S) have been assessed separately in consistency with the available experimental data. The fundamental properties at room temperatures (H298, S298) have been assessed in consistency with all other data. The liquid, bcc_A2 and tet phases () have been described by a simple substitutional model, with the formula (Fe1, U1)(). A realistic extrapolation of the excess Gibbs energy of the liquid phase at high temperature is proposed. The gas phase has been described by an ideal mixture of gaseous species, with the formula (Fe1, U1)1(G).

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- the activity of iron and uranium are in satisfactory agreement with the experimental ones in the liquid state ;

- the calculated and experimental phase diagrams are in very satisfactory agreement.

Figure 1	Calculated Fe-U phase diagram with special points and invariant reactions.

Figure 2 	Calculated Fe-U phase diagram compared with selected experimental data.

[1950Gro]	"The uranium-iron system"

J.D.Grogan,C.J. Birkett Clews,

Journal of the Institute of Metals, Vol.77, pp.571-580, (1950).

[1950Gor]	" "

P.Gordon, A.R.Kaufmann,

Transactions of the AIME, Vol.188, pp.182-194, (1950).

[1958Bel]	" "

J.Bellot, A.Blanchon, R.Chazot, P.Dosiere, J.M.Henry, M.Colas,

Comptes Rendus, Vol.246, pp. 3063-3065, (1958).

[1963Kha]	" "

D.K.Khakimova, Yu.S.Virgilev, O.S.Ivanov,

in O.S. Ivanov (ed.), "Stroenie i Svoistva Splavov Urana, Toriya i Tsirkoniya", 5-8, Gosatomizdat, Moiscow, (1963).

[1964Str]	" ",

J.A.Straatmann, N.F.Neumann,

U.S. At. Energy Comm. MCW-1487, 23p (1964).

[1964Rus]	" "

R.B.Russel,

U.S. At. Energy Comm. NMI-2813, 44p (1964).

[1964Ang]	" "

C.L.Angerman,

U.S. At. Energy Comm. DPST-64-219 (1964).

[1965Swi]	"The solubility of iron in solid uranium between 0.003 wt % and 0.3 wt % iron"

N.Swindells,

Journal of Nuclear Materials, Vol.18, pp.261-271, (1966).

[1966Mic]	" "

G.G.Michaud,

Canadian Metallurgical Quarterly, Vol.5, p.355, (1966).

[1973Leb]	"Thermodynamic properties of U-Fe alloys"

V.A.Lebedev, N.V.Nazarov, V.I.Pyatkov, I.F.Nichkov, S.P.Raspopin,

Izvestia Akademii Nauk SSSR, Metally, Vol.2, pp.212-216, (1973).

[1984Cha]	"Revision of the uranium-iron phase diagram"

L.R.Chapman, C.E.Holcombe, Jr.,

Journal of Nuclear Materials, Vol.126, pp.323-326, (1984).

[1991Lei]	"Thermodynamics and phase equilibria of the iron-uranium system"

L.Leibowitz, R.A.Blomquist,

Journal of Nuclear Materials, Vol.184, pp.47-52, (1991).

[1991Gar]	"Thermodynamique des alliages (U,Fe) et (U,Ga) en spectrométrie de masse à haute température"

P.Gardie, J.J.Poupeau, G.Bordier, J.Le Ny,

Calorim. Anal. Therm., Vol.22, pp.69-76, (1991).

FE-ZR

The phase diagram of the Fe-Zr binary system presents the following condensed solutions and substances, with the symbols used in this work or found in open literature :

- the liquid phase, L, which shows a complete miscibility from iron to zirconium ;

- the intermetallic compounds, Fe765Zr265(S), Fe1Zr2(S), Fe1Zr3(S) ;

- the intermediate non-stoichiometric Laves phase, Fe2Zr1(Laves) ;

- the terminal iron-rich solid solutions, bcc_A2 and fcc_A1, with a small solubility of zirconium ;

- the terminal zirconium rich solution, bcc_A2, with a limited solubility of iron ;

- the terminal zirconium rich solution, with the hexagonal closed packed structure, hcp_A3, and a very small solubility of iron.

The heat capacity (Cp) of the stoichiometric compounds Fe2Zr1(Laves), Fe1Zr2(S), Fe1Zr3(S) have been estimated from the Neuman-Kopp rule. The fundamental properties at room temperatures (H298, S298) have been assessed in consistency with all other data. The liquid, bcc_A2 and fcc_A1 phases () have been described by a simple substitutional model, with the formula (Fe1,Zr1)(). The Laves phase has been described with a two sublattice model, with the formula (Fe1, Zr1)2(Fe1, Zr1)1. A realistic extrapolation of the excess Gibbs energy of the liquid phase at high temperature is proposed. The gas phase has been described by an ideal mixture of gaseous species, with the formula (Fe1, Zr1, Zr2)1(G).

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- the activity of iron and zirconium are in satisfactory agreement with the experimental ones in the liquid state ;

- the selected enthalpy of mixing of the liquid phase is incompatible with the liquidus shape in the zirconium rich region ;

- the calculated and experimental phase diagrams are in satisfactory agreement : the non-stoichiometry.. range of the Laves phase and the temperatures of the invariant reactions are perfectly reproduced ; the liquidus shape in the zirconium rich region should be improved.

Figure 1	Calculated Fe-Zr phase diagram with special points and invariant reactions.

Figure 2	Calculated Fe-Zr phase diagram compared with selected experimental data.

[1931Vog]	"The Fe-Zr system"

R.Vogel, W.Tonn,

Archiv fuer EisenHuttenwesen, Vol.5, pp.387-389, (1931-1932).

[1951Hay]	"Constitution and mechanical properties of zirconium iron alloys"

E.T.Hayes, A.H.Robertson, W.L.O'Brien,

Transactions of the ASM, Vol.43, pp.888-897, (1951).

[1959Tan]	"Observations on the system zirconium-iron"

L.E.Tanner, D.W.Levinson,

Transactions of the Metallurgical Society of AIME, Vol.215, pp.1066-1067, (december 1959).

[1963Sve]	"Intermediate phases in the iron-zirconium system"

V.N.Svechnikov, V.M.Pan, A.Ts.Spektor,

Russian Journal of Inorganic Chemistry, Vol.8, N.9, pp.1106-1109, (September 1963).

[1969Shu]	"Constitution of binary alloys, second supplement"

F.A.Shunk,

MacGraw-Hill Book Company, New-York, St Louis, San Francisco, London, Sydney, Toronto, Mexico, Panama, 1969.

[1981Mal]	"The Zr-Fe phase diagram in the range 20-40 at% Fe and the crystalline structure of the intermetallic compound Zr3Fe"

T.O.Malakhova, Z.M.Alekseyeva,

J. Less Com. Met., vol.81, pp.293-300 (1981).

[1982Mal]	"The Zr-Fe phase diagram (0-66.6 at% Fe)"

T.O.Malakhova, A.N. Kobylin,

Russian Metallurgy, vol.2, pp.205-209 (1982).

[1985Stu]	"Determination of Fe solubility in alpha-Zr by Mossbauer spectroscopy"

M.M.Stupel, M.Bamberger, B.Z.Weiss,

Scripta Metallurgica, Vol.19, pp.739-740, (1985).

[1988Ari]	"The Fe-Zr (Iron-Zirconium) system"

D.Arias, J.P.Abriata,

Bulletin of Alloy Phase Diagrams, Vol.9, N.5, pp.597-604, (1988).

[1989Ale]	"The Zr-Fe phase diagram"

Z.M. Alekseeva, N.V. Korotkova,

Izvestiya Akademii Nauk SSSR. Metally, vol.4, pp.202-208 (1989).

[1990Bor]	"Study of the solubility of iron in zirconium by thermo-electric power measurements"

R.Borrelly, P.Merle, L.Adamy,

Journal of Nuclear Materials, Vol.170, pp.147-156, (1990).

[1993Bha]	"Modification of zirconium-iron phase diagram"

K.Bhanumurthy, G.B.Kale,

Scripta Metallurgica et Materialia, Vol.28, pp.753-756, (1993).

[1994Zou]	"The solid solubility of Fe in alpha-Zr : a secondary ion mass spectrometry study"

H.Zou, G.M.Hood, J.A.Roy, R.J.Schultz and J.A.Jackman,

Journal of Nuclear Materials, Vol.210, pp.239-243, (1994).

[1995Ser]	Experimental and thermodynamic assessment of the Fe-Zr system.

C. Servant, C. Guéneau, I. Ansara,

J. Alloys and Compounds, vol.220, N°1-2, pp. 19-26 (1995).

[1996Gra]	"Intermetallic phases in the iron-rich region of the Zr-Fe phase diagram"

M.S.Granovsky, D.Arias,

Journal of Nuclear Materials, Vol.229, pp.29-35, (1996).

[2002Ste]	"Experimental determination of intermetallic phases, phase equilibria, and invariant reaction temperatures in the Fe-Zr system",

F. Stein, G. Sauthoff, M. Palm,

J. Phase Equilibria, Vol. 23, N°6, pp. 480-494 (2002).

O-U

The phase diagram of the O-U binary system presents the following condensed solutions and substances, with the symbols used in this work or found in open literature :

- the liquid phase, L, which shows a miscibility gap between an UO2 rich liquid (L1) and an uranium rich liquid (L2) ;

- the intermediate solid oxides, O3U1(S) or UO3, O8U3(S) or U3O8-z, O9U4(S) or U4O9-y ; the compounds U5O13+x, U8O21, UO2.61, have also been cited ;

- the oxide solid solution, UO2+x, with the face-centred cubic structure, of CaF2 (fluorite) type, Fm3m, cF12, noted fcc_C1 ;

- pure solid uranium, with a negligible solubility of oxygen, and different allotropic structures, orthorhombic, U1(ort_A20), tetragonal, U1(tet), and body cubic centred, U1(bcc_A2) ;

- the gas phase, which shows an extended solubility of uranium above 2000 K.

The fundamental thermodynamic properties (Cp, H298, S298) of the stoichiometric compounds O3U1(S), O8U3(S), O9U4(S) and O2U1(S) have been assessed separately in consistency with the available experimental data.  The liquid phase has been described by a non-ideal associate model, with the formula (O1, O2U1, U1)(L), and the solid solution UO2+x by a three sublattice model, with the formula (U1)1(O1, □)2(O1, □)1(fcc_C1). In order to be compatible with the whole thermodynamic database and to allow the introduction of iron, the model has been simplified in a simple one lattice model, with the formula (O1, O2U1, U1)1(fcc_C1). The gas phase has been described by an ideal mixture of gaseous species, with the formula (O1, O1U1, O2U1, O2, O3, O3U1, U1)1(G).

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- the oxygen potential experimental database is perfectly reproduced in the UO2+x region, while the calculated curvature is stronger than the experimental one in the UO2-x region, especially with the simplified model. However, the values in the diphasic domains are in good agreement ;

      - the phase equilibria (solid UO2+x region, liquidus, miscibility gap tie line) are well represented, but the UO2+x region at high temperature has to be experimentally validated. The non-stoichiometry range of U3O8-z and U4O9-y have not been taken into account. The hypothesis of a small solubility of oxygen in liquid uranium has been retained.

Figure 1	Calculated O-U phase diagram with special points and invariant reactions.

Figure 2	Calculated O-U phase diagram compared with selected experimental data.

[1963Blu]	"Sur le système binaire uranium-dioxyde d'uranium"

P.L. Blum, P. Guinet et H. Vaugoyeau,

C.R. Acad. Sciences, T. 257, No. 22, pp. 3401-3403 (1963).

[1965Mar]	"	"

A.E. Martin and R.K. Edwards,

J. Phys. Chem., 69, 5 (1965) 1788 ; R. K. Edwards and  A.E. Martin, p. 423 in Thermodynamics of Nuclear Materials", Vol. II, IAEA, Vienna, 1966.

[1966Gui]	"Le système binaire uranium-dioxyde d'uranium au-dessus de 1130°C"

P. Guinet, H. Vaugoyeau et P.L. Blum,

C.R. Acad. Sciences, T. 263, Série C, pp. 17-20 (1966).

[1967Ban]	"Melting Temperatures in the System Uranium-Uranium dioxide"

M.J. Bannister,

Journal of Nuclear Materials, 24 (1967) 340-342.

[1968Kot]	"Détermination des limites de phases du système U-O par transfert d'oxygène. Diagramme de phases pour la région 2.19<O/U<2.653 et 1080°C<T<1200°C.

A. Kotlar, P. Gerdanian et M. Dode,

J. Chem. Phys., 65, 687-691 (1968).

[1969Ack]	"A Thermodynamic Study of the Urania-Uranium System"

R.J. Ackermann, E.G. Rauh and M.S. Chandrasekharaiah,

The Journal of Physical Chemistry, 73, 4 (1969) 762-769.

[1970Lat]	"Détermination of Solidus-Liquidus Temperatures in the  UO(2+x) System (- 0.50 < x < 0.20)"

R.E. Latta and R.E. Fryxell,

Journal of Nuclear Materials, 35 (1970) 195-210.

[1970Tet]	"Total pressure of uranium-bearing species over oxygen-deficient urania"

M. Tetenbaum and P.D. Hunt,

Journal of Nuclear Materials, 34 (1970) 86-91.

[1974Sai]	"Non-stoichiometry in uranium dioxide"

Y. Saito,

Journal of Nuclear Materials, 51 (1974) 112-125.

[1975Mat]	"Phase relation and defect structures of nonstoichiometric U4O9+-y and UO2+x at high temperatures"

T. Matsui and K. Naito,

Journal of Nuclear Materials, 56 (1975) 327-335.

[1980Gar]	"Solubility of Oxygen in Liquid Uranium and the Composition of the Lower Phase Boundary of Uranium Dioxide at 1950 K"

S.P.Garg and R.J.Ackermann,

Journal of Nuclear Materials, Vol. 88, pp. 309-311 (1980).

[1998Gue]	"Liquid immiscibility in a (O,U,Zr) model corium"

C. Gueneau, V. Dauvois, P. Perodeaud, C. Gonella, O. Dugne,

Journal of Nuclear Materials, 254 (1998) 158-174.

[2005Man] 	"Melting of stoichiometric and hyperstoichiometric uranium dioxide"

D. Manara, C. Ronchi, M. Sheindlin,

Journal of Nuclear Materials, 342 (2005) 148-163.

Figure 3 	Calculated UO2+x solid region compared with selected experimental data.

[1958Bla]	" "

P.E. Blackburn,

J. Phys. Chem., 62, 8 (1958) 897-902.

[1960Sch]	" "

B.E. Schaner,

J. Nucl. Mater., 2,2 (1960) 110-120.

[1961Rob]	" "

L.E. Roberts and A.J. Walter,

J. Inorg. Nucl. Chem., 22 (1961) 213-229.

[1961Aro]	" "

S. Aronson, J.E. Rulli and B.E. Schaner,

J. Chem. Phys. 35, 4 (1961) 1382-1388

[1963Ant] 	" "

A.M. Anthony, R. Kiyoura and T. Sata,

J. Nucl. Mater. 10, 1(1963) 8-14.

[1966Hag]	"Equilibrium oxygen pressures Over the non-stoichiometric uranium oxides UO2+x and U3O8-z at higher temperatures"

K. Hagemark and M. Broli,

J. Inorg. Nucl. Chem., 28 (1966) 2837-2850.

[1968Kot]	"Détermination des limites de phases du système U-O par transfert d'oxygène. Diagramme de phases pour la région 2.19<O/U<2.653 et 1080°C<T<1200°C.

A. Kotlar, P. Gerdanian et M. Dod‚,

J. Chem. Phys., 65, 687-691 (1968).

[1970Lie]	" "

W.V. Lierde, J. Pelsmaekers and A. Lecoq-Robert,

J. Nucl. Mater. 37 (1970) 276-285.

[1970Ish]	" "

T. Ishii, K. Naito and K. Oshima,

Solid State Communications 8 (1970) 677-683.

1974Sai]	"Non-stoichiometry in uranium dioxide"

Y. Saito,

Journal of Nuclear Materials, 51 (1974) 112-125.

[1974Ban]	"A dilatometric study of the solubility of U4O9 in UO2"

M.J. Bannister and W.J. Buykx,

Journal of Nuclear Materials, 55 (1974) 345-351.

[1975Mat]	" "

T. Matsui and K. Naito,

Journal of Nuclear Materials, 56 (1975) 327-335.

[1978Dha]	" "

S.R. Dharwadkar, M.S. Chandrasekharaiah and M.D. Karkhanavaia,

Journal of Nuclear Materials, 71 (1978) 268-276.

[1981Pic]	 " "

C. Picard and P. Gerdanian,

Journal of Nuclear Materials, 99 (1981) 184-189.

[1984Can]	" "

A. Caneiro and J.P. Abriata,

Journal of Nuclear Materials, 126 (1984) 255-267.

[1987Nak]	"Thermodynamic study of UO2+x by solid state emf technique"

A. Nakamura and T. Fujino,

Journal of Nuclear Materials, 149 (1987) 80-100.

Figure 4	Calculated UO2+x region compared with selected experimental data.

[1963Blu]	"Sur le système binaire uranium-dioxyde d'uranium"

P.L. Blum, P. Guinet et H. Vaugoyeau,

C.R. Acad. Sciences, T. 257, No. 22, pp. 3401-3403 (1963).

[1965Mar]	" "

A.E. Martin and R.K. Edwards,

J. Phys. Chem., 69, 5 (1965) 1788  ; R. K. Edwards and  A.E. Martin, p. 423 in Thermodynamics of Nuclear Materials", Vol. II, IAEA, Vienna, 1966.

[1966Gui]	"Le système binaire uranium-dioxyde d'uranium au-dessus de 1130°C"

P. Guinet, H. Vaugoyeau et P.L. Blum,

C.R. Acad. Sciences, T. 263, Série C, pp. 17-20 (1966).

[1967Ban]	"Melting Temperatures in the System Uranium-Uranium dioxide"

M.J. Bannister,

Journal of Nuclear Materials, 24 (1967) 340-342.

[1968Kot]	"Détermination des limites de phases du système U-O par transfert d'oxygène. Diagramme de phases pour la région 2.19<O/U<2.653 et 1080°C<T<1200°C.

A. Kotlar, P. Gerdanian et M. Dode,

J. Chem. Phys., 65, 687-691 (1968).

[1969Ack]	"A Thermodynamic Study of the Urania-Uranium System"

R.J. Ackermann, E.G. Rauh and M.S. Chandrasekharaiah,

The Journal of Physical Chemistry, 73, 4 (1969) 762-769.

[1970Lat]	"Determination of Solidus-Liquidus Temperatures in the UO(2+x) System (-0.50<x<0.20)"

R.E. Latta and R.E. Fryxell,

Journal of Nuclear Materials, 35 (1970) 195-210.

[1970Tet]	"Total pressure of uranium-bearing species over oxygen-deficient urania"

M. Tetenbaum and P.D. Hunt,

Journal of Nuclear Materials, 34 (1970) 86-91.

1974Sai]	"Non-stoichiometry in uranium dioxide"

Y. Saito,

Journal of Nuclear Materials, 51 (1974) 112-125.

[1975Mat]	"Phase relation and defect structures of nonstoichiometric U4O9+-y and UO2+x at high temperatures"

T. Matsui and K. Naito,

Journal of Nuclear Materials, 56 (1975) 327-335.

[1980Gar]	"Solubility of Oxygen in Liquid Uranium and the Composition of the Lower Phase Boundary of Uranium Dioxide at 1950 K"

S.P.Garg and R.J.Ackermann,

Journal of Nuclear Materials, Vol. 88, pp. 309-311 (1980).

[1998Gue]	"Liquid immiscibility in a (O,U,Zr) model corium"

C. Gueneau, V. Dauvois, P. Perodeaud, C. Gonella, O. Dugne,

Journal of Nuclear Materials,  254 (1998) 158-174.

[2005Man] 	"Melting of stoichiometric and hyperstoichiometric uranium dioxide"

D. Manara, C. Ronchi, M. Sheindlin,

Journal of Nuclear Materials, 342 (2005) 148-163.

O-ZR

The phase diagram of the O-Zr binary system presents the following condensed solutions and substances, with the symbols used in this work or found in open literature :

- the liquid phase, L, which shows a complete miscibility from O2Zr1 oxide to Zr metal ;

- the pure solid oxides, with the allotropic forms monoclinic O2Zr1(mon) and tetragonal O2Zr1(tet) ;

- the oxide solid solution, ZrO2-x, with the face-centred cubic structure, of CaF2 (fluorite) type, Fm3m, cF12, noted fcc_C1 ;

- the terminal zirconium rich solid solutions, body cubic centred (bcc_A2), and hexagonal closed packed (hcp_A3) pure solid uranium, with a solubility of oxygen limited to about 10 at% and 30 at% respectively ;

- the gas phase, which shows an extended solubility of zirconium above 3000 K.

The fundamental thermodynamic properties (Cp, H298, S298) of the stoichiometric compound O2Zr1(mon, tet, fcc_C1) have been assessed separately in consistency with the available experimental data. The liquid phase has been described by a non ideal associate model, with the formula (O1, O2Zr1, Zr1)1(L), and the solid solution ZrO2-x, bcc_A2 and hcp_A3 by three and two sublattice models, with the respective formula (Zr1)1(O1, □)2((O1, □)1(fcc_C1), (Zr1)1(O1, □)3(bcc_A2), and (Zr1)1(O1, □)0.5(hcp_A3). In order to be compatible with the whole thermodynamic database and to allow the introduction of iron, the model of the fcc_C1 solid solution has been simplified in a simple one lattice model, with the formula (O1, O2Zr1, Zr1)1(fcc_C1). The gas phase has been described by an ideal mixture of gaseous species, with the formula (O1, O1Zr1, O2, O2Zr1, O3, Zr1, Zr2)1(G).

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- the oxygen potential experimental database is correctly reproduced in the monophasic regions ZrO2-x, fcc_C1 and hcp_A3, while some disagreements have been observed in the diphasic region fcc_C1+hcp_A3 ;

- the phase equilibria (solid ZrO2-x region, diphasic regions O2Zr1(mon, tet) + hcp_A3, fcc_C1 + hcp_A3, hcp_A3 + bcc_A2) are well represented, but the liquidus L + ZrO2-x should be validated ;

      - several stoichiometric oxides observed in the zirconium rich domain at low temperature (T < 750 K) could be included.

Figure 1	Calculated O-Zr phase diagram with special points and invariant reactions.

Figure 2	Calculated O-Zr phase diagram compared with selected experimental data.

[1954Dom]	"System zirconium-oxygen"

R.F.Domagala and D.J.McPherson

Journal of Metals, Transactions of the AIME, 238-246, February 1954.

[1961Hol]	"X-Ray studies on solid solutions of oxygen in alpha-zirconium"

Bo Holmberg and Tore Dagerhamn

Acta Chemica Scandinavica, Vol.15, N.4, 919-925, (1961).

[1961Geb]	“Research on the system zirconium-oxygen”

E.Gebhardt, H.D.Seghezzi and W.Duerrschnabel

Journal of Nuclear Materials, Vol.4, N.3, 255-268, (1961).

[1967Ruh]	"Non-stoichiometry of ZrO2 and its relation to tetragonal-cubic inversion in ZrO2"

R.Ruh and H.J.Garrett,

Journal of the American Ceramic Society, Vol.50, N.5, 257-261, (1967)

[1977Ack]	 "High-temperature phase diagram for the system Zr-O"

R.J.Ackermann, S.P.Garg, E.G.Rauh

Journal of The American Ceramic Society, Vol.60, N°.7-8, 341-345, (1977).

[1978Ack]	"The lower phase boundary of ZrO2-x"

R.J.Ackermann, S.P.Garg, E.G.Rauh

Journal of The American Ceramic Society, Vol.61, N.5-6, 275-276, (1978).

[1987Tan]	"AES and XPS studies of oxygen stabilized alpha zirconium"

T.Tanabe, M.Tanaka and S.Imoto

Surface Science, Vol.187, 499-510, (1987).

[1998Ves]	"Analysis of the FZK previous tests and pre-test calculations of the FZK new tests on ZrO2 dissolution by molten zircaloy"

M.Veshunov

In vessel cluster INV-CIT(98)-M006, IPSN/DRS/SEMAR 98/36, Minutes of the 4th CIT project meeting, Pisa (10th and 11th June 1998) ; M.Barrachin and B.Adroguer.

[1999Lia]	"Thermodynamic assessment of the O-Zr system"

P. Liang, H. Seifert, H.L. Lukas, S. Fries, N. Dupin, I. Ansara and F. Aldinger,

Calphad XXVII.

U-ZR

The phase diagram of the U-Zr binary system presents the following condensed solutions and substances, with the symbols used in this work or found in open literature :

- the liquid phase, L, which shows a complete miscibility from uranium to zirconium ;

- the body cubic centred solid solution, bcc_A2, with also a complete miscibility at high temperature and a small miscibility gap deported on the uranium side between 950 K and 1000 K ;

- the terminal solid solutions, uranium rich orthorhombic and tetragonal, ort_A20 and tet, with a small solubility of zirconium, and zirconium rich hexagonal closed packed, hcp_A3, with a small solubility of uranium ;

- the intermetallic solid solution, , which extents from 64 to 78 at% Zr.

The liquid, bcc_A2, ort_A20, tet and hcp_A3 phases () have been described by a simple substitutional model, with the formula (U1, Zr1)(, and the intermetallic solid solution by a two sublattice model, with the formula (U1, Zr1)2(Zr1)(). The gas phase has been described by an ideal mixture of gaseous species, with the formula (U1, Zr1)1(G). The excess Gibbs energy of the liquid and bcc_A2 solid solution has been assessed more physically than in other assessments found in open literature.

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- some experimental activities were found to be too negative and discarded for experimental reasons (interaction with crucible, impurities) ;

- the calculated phase diagram is in satisfactory agreement with the experimental one ;

  - thermodynamic properties in the liquid phase should be determined at high temperature.

Figure 1	Calculated U-Zr phase diagram with special points and invariant reactions.

Figure 2	Calculated U-Zr phase diagram compared with selected experimental data.

[1954Sum]	"The Constitution of Uranium-Zirconium Alloys"

D.Summers-Smith,

Journal of the Institute of Metals, Vol.83, pp.277-282, (1954-55).

[1957Phi]	"Etablissement des diagrammes d'équilibre des alliages binaires par des expériences de diffusion intermétalliques. Application au système uranium-zirconium"

J.Philibert, Y.Adda,

Comptes Rendus de l'Académie des Sciences, pp.2507-2510, (23 décembre 1957).

[1958Duf] 	"Delta phase field of the U-Zr equilibrium diagram"

J.F.Duffey, C.A.Bruch,

Transactions of the Metallurgical Society of AIME, 17-19, (Février 1958).

[1958How]	" "

B.W.Howlett, A.G.Knapton,

2nd UN Internatinal Conference on Peaceful Use of Atomic Energy, Geneva, Vol.6, p.104, (1958).

[1962Zeg]	"The uranium-rich end of the uranium-zirconium system"

S.T.Zegler,

USAEC Rep.ANL-6055 (1962).

[1988Kan]	"Thermodynamic activity measurements of U-Zr alloys by Knudsen effusion mass spectrometry"

M.Kanno, M.Yamawaki, T.Koyama, N.Morioka,

Journal of Nuclear Materials, Vol. 154, pp.154-160, (1988).

[1989Lei]	"Thermodynamics of the uranium-zirconium system"

L.Leibowitz, R. A.Blomquist, A.D.Pelton,

Journal of Nuclear Materials, Vol. 167, pp.76-81, (1989).

[1991Ohm]	" "

T.Ohmichi,

private communication, reported by T. Ogawa, T. Iwai, Journal of the Less-Common Metals, vol.170, pp.101-108 (1991).

[1992Mae]	" "

A.Maeda, Y.Suzuki,T.Ohmichi,

Journal of Alloys and Compounds, Vol. 179, L21-24, (1992).

[1992Aka]	"Stability and structure of the delta phase of the U-Zr alloys"

M.Akabori, A.Itoh, T.Ogawa, F.Kobayashi, Y.Suzuki,

Journal of Nuclear Materials, Vol. 188, pp .249-254, (1992).

Figure 3	Partial calculated U-Zr phase diagram compared with selected experimental data.

[1954Sum]	"The constitution of uranium-zirconium alloys"

D.Summers-Smith,

Journal of the Institute of Metals, Vol. 83, pp.277-282, (1954-55).

[1957Phi]	"Etablissement des diagrammes d'équilibre des alliages binaires par des expériences de diffusion intermétalliques. Application au système uranium-zirconium"

J.Philibert, Y.Adda,

Comptes Rendus de l'Académie des Sciences, pp.2507-2510, (23 décembre 1957).

[1958How]	" "

B.W.Howlett, A.G.Knapton,

2nd UN International Conference on Peaceful Use of Atomic Energy, Geneva, Vol. 6, p.104, (1958).

[1958Duf]	"Delta phase field of the U-Zr equilibrium diagram"

J.F.Duffey, C.A.Bruch,

Transactions of the Metallurgical Society of AIME, 17-19, (Février 1958).

[1962Zeg]	"The Uranium-rich end of the uranium-zirconium system"

S.T.Zegler,

USAEC Rep.ANL-6055 (1962).

[1992Aka]	"Stability and structure of the delta phase of the U-Zr alloys"

M.Akabori, A.Itoh, T.Ogawa, F.Kobayashi, Y.Suzuki,

Journal of Nuclear Materials, Vol. 188, pp. 249-254, (1992).

O2U1-O2ZR1

The phase diagram of the O2U1-O2Zr1 pseudo-binary system presents the following condensed solutions and substances, with the symbols used in this work or found in open literature :

- the liquid phase, L, which shows a complete miscibility from O2U1 oxide to O2Zr1 oxide ;

- the pure solid oxide, with the allotropic form monoclinic, O2Zr1(mon) ;

- the oxide solid solution, (U, Zr)O2, with the face-centred cubic structure, of CaF2 (fluorite) type, Fm3m, cF12, noted fcc_C1 ;

- the terminal O2Zr1 rich solid solutions, tetragonal (tet_oxide),  with a solubility of O2U1 limited to about 23 mol%.

The fundamental thermodynamic properties (Cp, H298, S298) of the stoichiometric compounds O2U1(fcc_C1) and O2Zr1(mon, tet, fcc_C1) have been assessed separately in consistency with the available experimental data. The liquid, fcc_C1 and tetragonal phases () have been described by a simple substitutional model, with the formula (O2U1, O2Zr1)1(), which is compatible with the two sublattice model (U1, Zr1)O2().

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- the experimental activity of O2U1 and O2Zr1 in the fcc_C1 and tetragonal solid solutions are satisfactorily reproduced ;

  - the calculated phase diagram is in good agreement with the experimental data.

Figure 1	Calculated O2U1-O2Zr1 pseudo-binary phase diagram with special points and invariant reactions.

Figure 2	Calculated O2U1-O2Zr1 pseudo-binary phase diagram compared with selected experimental data.

[1953Lam]	"Uranium oxide phase equilibrium systems"

W.A. Lambertson, M.H. Muller,

J. Am. Cer. Soc., vol.36, N°11, p.365 (1953).

[1958Vor]	 "Phase equilibrium diagrams of the UO2-ZrO2 and ThO2-ZrO2 Systems"

N. M. Voronov, E.A. Voitekhova and A.S. Danilin,

Proc. 2nd Genova Conf., Vol. 6, pp.221-225, (1958).

[1960Eva]	"The system UO2-ZrO2"

P.E. Evans,

J. Am. Ceram. Soc, 43, vol.9, pp.443-447 (1960).

[1963Wis]	" "

L. G. Wisnyi and S. W. Pijanowsko,

Knolls Atomic Power Laboratory (U.S.A.) Report, KAPL-1702 (1957).

[1963Coh]	"A metallographic and x-ray study of the UO2-ZrO2 system"

I. Cohen, B.E. Schaner,

J. Nucl. Mat., Vol.9, N°1, pp.18-52 (1963).

[1967Rom]	"Phase equilibrium studies in the UO2-ZrO2 system"

K.A. Romberger, C.F. Baes and H.H. Stone,

J. Inorg. Nucl. Chem., Vol. 29, pp.1619-1630 (1967).

[1983Une]	"Oxygen potential of U0.85Zr0.15O2+x solid solutions at 1500C"

K. Une, M. Oguma,

J. Amer. Ceram. Soc., Vol. 66, pp.179-180 (1983).

[1987Pas]	"Phase equilibria in the BaO-UO2-ZrO2-MoO2 system"

J.O.A. Pashoal, H. Kleykamp and F. Thümmler,

J. Nucl. Mat., Vol.151, pp.10-21 (1987).

[2001Pun]	"Determination of the solidus and liquidus temperatures of uranium-zirconium oxides"

J.S. Punni, M.A. MIignanelli,

ENTHALPY Project, SAM-ENTHA(01)-D004, August 2001.

[2001Bai]	"Mass spectrometric study of UO2-ZrO2 pseudo-binary system"

M. Baichi, C. Chatillon, C. Guéneau, S. Chatain,

Journal of Nuclear Materials, Vol. 294, pp. 84-87 (2001).

FE-O-U

The phase diagram of the Fe-O-U ternary system presents the following solutions and substances, with the symbols used in this work :

  - the liquid phase, L, which shows a miscibility gap between an Fe-U-O rich metal-oxygen liquid (L1) and a FeO-Fe2O3-UO2 rich oxide liquid (L2) ; it extends from the Fe-O side to the O-U side it could present a miscibility gap between a Fe2O3/Fe3O4 rich phase (L2) and a UO2 rich liquid (L3) ;

  - the oxide solid solution, (U,Fe)O2+x, with the face-centred cubic structure, of CaF2 (fluorite) type, Fm3m, cF12, noted fcc_C1,  and which can dissolves until 15 mol% FeO in UO2 ;

  - the oxide solid solution, FeO1+x, or wustite, with the face-centred cubic structure, of NaCl type, noted fcc_B1 ; no solubility of urania in wustite is reported ;

  - the uranium rich terminal solid solutions, tetragonal, tet_metal, and body cubic centred, bcc_A2, with a small solubility of iron.

  - the pure solid oxides, Fe3O4(S) or magnetite, Fe2O3(S) or hematite, corundum, O3U1(S), O8U3(S), O9U4(S) ;

  - the inter-metallic compounds, Fe2U1(S) with the Laves structure, and Fe1U6(S) ;

  - the ternary solid oxide,  Fe1O4U1(S) ;

  - pure solid iron, with a negligible solubility of oxygen and uranium, and  two allotropic structures, body cubic centred, Fe1(bcc_A2), and cubic face centred, Fe1(fcc_A1) ;

  - pure orthorhombic uranium U1(ort_A20),  with a negligible solubility of iron and oxygen ;

  - the gas phase (G), which shows an extended solubility in oxygen of iron  above 2800 K and of uranium above 2000 K.

The fundamental thermodynamic properties (Cp, H298, S298) of the stoichiometric compounds Fe0.947O1(fcc_B1), Fe3O4(S), Fe2O3(S), O3U1(S), O8U3(S), O9U4(S), O2U1(fcc_C1) have been assessed in the individual sub-systems, as well as the thermodynamic modelling of all binary or pseudo-binary phases. The ternary liquid phase has been described by a non- ideal associate model, with the formula (Fe1, Fe1O1, Fe1O1.5, O1, O2U1, U1)1(L). The fcc_C1 and fcc_B1 solid solutions have been described will a one lattice model, with the formula (Fe1O1,O2U1)1(fcc_C1) and (Fe1O1, Fe1O1.5)1(fcc_B1) respectively. The Gibbs energy of the ternary solid oxide Fe1O4U1(S) has been assessed from the experimental information (thermodynamics and phase diagram). The gas phase has been described by an ideal mixture of gaseous species, with the formula (Fe1, Fe1O1, Fe1O1.5, O1, O1U1, O2, O2U1, O3, O3U1, U1)1 (G).

In the metal-oxygen field, the only used experimental information [1997Kle] on phase diagram is located on the line Fe-UO2 and indicate a very low solubility of UO2 in liquid iron at very high temperature (2873 K).

In the ternary oxide field, the Fe1O4U1(S) was found to be decomposed at 1310 K.

Most of the more recent experimental informations are located in the pseudo-binary vertical sections, FeO-UO2 ([1998Hel], [2003Pet], [2004Cor]) and Fe2O3/Fe3O4-UO2 ([1969Ril], [2005Kis]), and come from the CORPHAD and SARNET international projects.

The main features of the FeO-UO2 isopleth to section [2004Cor] are a complete solubility between FeO and UO2 in the oxide liquid (L2), and a non negligible solubility of iron oxide in the UO2 rich fcc_C1 solid solution. The eutectic point was experimentally assessed as T = 1615 K (1342°C) and 4 mol% UO2 (13.6 wt%). The solubility of iron oxide in fcc_C1 at the eutectic temperature was assessed as 17 mol% FeO (5 wt%).

The Fe2O3/Fe3O4-UO2+x isopleth section has been experimentally studied in air [1969Ril], and its edges vary with composition from UO2+x, U3O8 or U4O8 below 2126 K and 1394 K, and from Fe2O3 to Fe3O4 (melting point, 1869 K) above 1730 K ; according to Riley [1969Ril], the eutectic reaction L  U3O8 + Fe2O3 is located at 1513 K (1240 °C) and 30 wt% Fe2O3, 70 wt% UO2, corresponding to 59.2 mol% Fe1O1.5, 40.8 mol% UO2. Whatever, this diagram is still imprecise and presumption of a liquid miscibility gas was recently put in evidence by Kiselova and Petrov [2005Kis]. According to these authors, the eutectic L  UO2 + FeO1.33 was located at 1621 K (1348 °C) and 68.5 wt% UO2, 31.5 wt% Fe3O4, and a miscibility gap was found between 1673 K (1400 °C) and 1973 K (1700 °C) on the iron oxide rich side.

In a first approximation, the excess interaction parameters between Fe1O1 and O2U1 on the one hand and Fe1O1.5 and O2U1 on the other hand have been estimated by assuming the pseudo-binary sections as quasi-binary ones.

The real isothermal or isopleth sections may be then calculated from the complete thermodynamic modelling. The main features of the FeO-UO2 pseudo-binary system are qualitatively well reproduced, but the residual uncertainty on the Fe2O3/Fe3O4-UO2 pseudo-binary system leads to quantitative differences between re-calculated liquidus and experimental one, due to the presence of Fe1O1.5 species in the liquid phase.

The Fe2O3/Fe3O4-UO2 pseudo-binary system has been considered without the new assumption of a liquid miscibility gap and the corrected eutectic temperature [2005Kis].

Finally, the refinement of the liquid interaction parameters between Fe1O1 and O2U1 and Fe1O1.5 and O2U1 will be mainly linked to the improvement of the description of the Fe2O3/Fe3O4-UO2 pseudo-binary system.

At high temperatures (T > 2273 K), the ternary phase diagram is characterised by the following phase equilibria : L1 + fcc_C1, L1 + L2 + fcc_C1, L2 + fcc_C1, L2 + G, L2 + G + fcc_C1, L1 + L2.

[1969Ril]	Fe2O3-O2U1 "The UO2-Fe2O3 and PuO2-Fe2O3 Systems in Air"

B.Riley

Transactions of the American Nuclear Society, Vol.12, pp.543-544, (1969).

[1997Kle]	H. Kleykamp, “Phase equilibria in the UO2-austenitic steel system up to 3000 °C”

Journal of Nuclear Materials, 247, (1997), 103-107.

[1998Hel]	Fe1O1-O2U1 "The FeO-UO2 System"

S.Helmann, M.Nie,

In vessel cluster INV-CIT(98)-M006, IPSN/DRS/SEMAR 98/36, Minutes of the 4th CIT Project Meeting, Pisa, (10th and 11th June 1998).

[2003Pet]	Fe1O1-O2U1"Study of UO2-FeO system at induction melting in inert atmosphere"

Y. Petrov,

A.P. Alexandrov Research Institute, second CORPHAD Meeting, St Petersburg, September 17, 2003.

[2004COR,VPA/IMCC]

Fe1O1-O2U1 "System UO -FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2004COR,Galakhov]

Fe1O1-O2U1 "System UO -FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2004COR,Galakhov,discarded]

Fe1O1-O2U1 "System UO2-FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2004COR,IMCC/EDX]

Fe1O1-O2U1 "System UO2-FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2005Kis]	M. Kiselova, Y.B. Petrov, “New crystallization studies of UO2-ZrO2-Fe3O4 system and the presumed melting diagram“,

SARNET meeting, Köln, February 2005.

Figure 1	Calculated Fe-O-U isothermal section at 1273 K.

Figure 2	Calculated Fe-O-U isothermal section at 1773.15 K.

Figure 3	Calculated Fe-O-U isothermal section at 2273.15 K.

Figure 4	Calculated Fe-O-U isothermal section at 2273.15 K.

FE-O-ZR

The phase diagram of the Fe-O-Zr ternary system presents the following solutions and substances, with the symbols used in this work :

- the liquid phase, L, which shows a miscibility gap between an Fe-Zr rich metallic liquid (L1) and an FeO/Fe2O3-ZrO2 rich oxide liquid (L2) ; it extends from the Fe-O side and closes at zirconium rich content ; it may also exist a liquid miscibility gap in the oxide field, observed in the Fe2O3/Fe3O4-ZrO2 system between 2100 K and 2600 K, while there is a complete liquid miscibility in the FeO-ZrO2 system.

- the ZrO2 rich oxide solid solution, with the face-centred cubic structure, of CaF2 (fluorite) type, Fm3m, cF12, noted fcc_C1,  and which can dissolves until 18 mol% FeO in ZrO2 ;

- the ZrO2 rich oxide solid solution, with the tetragonal structure, noted tet_oxide,  and which can dissolve until 7 mol% Fe1O1.5 in ZrO2 ;

- the oxide solid solution, FeO1+x, or wustite, with the face-centred cubic structure, of NaCl type, noted fcc_B1 ; no solubility of zirconia in wustite is reported ;

- the terminal zirconium rich solid solution, body cubic centred (bcc_A2), with a solubility of oxygen limited to about 10 at% and a solubility of iron limited to 5 at% ;

- the terminal zirconium rich solid solution, hexagonal closed packed (hcp_A3) with a solubility of oxygen limited to about 30 at% and a very small solubility of iron ;

- the terminal iron-rich solid solutions, bcc_A2 and fcc_A1, with a small solubility of zirconium and a negligible solubility of oxygen ;

- the intermediate non-stoichiometric Laves phase, Fe2Zr1(Laves) ;

- the pure solid oxides, Fe3O4(S) or magnetite, Fe2O3(S) or hematite, corundum, O3U1(S), O8U3(S), O9U4(S) ;

- the intermetallic compounds, Fe765Zr265(S), Fe1Zr2(S), Fe1Zr3(S) ;

- the pure solid zirconium oxide, with the allotropic form monoclinic O2Zr1(mon) ;

- the gas phase (G), which shows an extended solubility in oxygen of iron above 2800 K and of zirconium above 3000 K.

The fundamental thermodynamic properties (Cp, H298, S298) of the stoichiometric compounds Fe0.947O1(fcc_B1), Fe1O1.5(S), Fe3O4(S), Fe2O3(S), O2Zr1(fcc_C1, tet, mon), Fe2Zr1(Laves), Fe765Zr265(S), Fe1Zr2(S), Fe1Zr3(S) have been assessed in the individual sub-systems, as well as the thermodynamic modelling of all binary or pseudo-binary phases. The ternary liquid phase has been described by a non ideal associate model, with the formula (Fe1,Fe1 O1,Fe1O1.5,O1,O2Zr1,Zr1)1(L).  The fcc_C1, tet_oxide and fcc_B1 solid solutions have been described with a one lattice model, whith the formula (Fe1O1,O2Zr1)1(fcc_C1), (Fe1O1,Fe1O1.5,O2Zr1)1(tet_oxide) and (Fe1O1,Fe1O1.5)(fcc_B1) respectively. The terminal iron-zirconium rich solid solutions, bcc_A2 and hcp_A3, have been described by a two-sublattice model, with the respective formula (Fe1,Zr1)1(O1,□)3(bcc_A2), and (Fe1,Zr1)1(O1,□)0.5(hcp_A3). The gas phase has been described by an ideal mixture of gaseous species, with the formula (Fe1, Fe1O1, Fe1O1.5, O1, O1Zr1, O2, O2Zr1, O3, Zr1, Zr2)1 (G).

In the metal-oxygen field, the only used experimental information on phase diagram is located on the line Fe-ZrO2 and gives the solubility of oxygen in iron rich-zirconium liquid alloys. (1873 K - 2073 K).

Most of the more recent experimental informations are located in the pseudo-binary vertical sections, FeO-ZrO2 ([1997Fis], [1998Hel], [1999Bec], [2003Gus], [2004Cor]) coming from the CORPHAD international project, and Fe2O3/Fe3O4-ZrO2 ([2003Pil], [2004Pet]) coming from the ECOSTAR international project.

The main features of the FeO-ZrO2 isopleth section [2004Cor] are a complete solubility between FeO and ZrO2 in the oxide liquid (L2), and a non negligible solubility of iron oxide in the ZrO2 rich fcc_C1 and tet_oxide solid solutions.

The eutectic temperature was located in the temperature range 1588 – 1603 K (1315 – 1330 °C) and the corresponding composition 10.26 mol% ZrO2 (16.4 wt%). The solubility of iron oxide in tetragonal ZrO2, tet_oxide, is about 2.2 mol% FeO (1.3 wt%) at the eutectic temperature. The solubility of iron oxide in cubic ZrO2, fcc_C1, is about 8-12 mol% FeO (5-7 wt%) in the temperature range 2073-2373 K (1800 – 2100 °C).

The Fe2O3/Fe3O4-ZrO2 isopleth section has been experimentally studied in the ECOSTAR project ([2003Pil], [2004Pet]). It shows a miscibility gap in the liquid state, located between the monotectic temperature 2143 K (1870 °C) and the critical point 2483 K (2210 °C), and an eutectic temperature at 1798 K (1525 °C). There is a non negligible solubility of FeO1.333 in tetragonal ZrO2, tet_oxide, the maximal one being about 6.6 wt% Fe3O4 at the monotectic temperature. The solid solubility of Fe3O4 in cubic ZrO2, fcc_C1, and of ZrO2 in Fe3O4 are less than 2.5 wt%.

In a first approximation, the excess interaction parameters between Fe1O1 and O2Zr1 on the one hand and Fe1O1.5 and O2Zr2 on the other hand have been estimated by assuming the pseudo-binary sections as quasi-binary ones. The real isothermal or isopleth sections may be than calculated from the complete thermodynamic modelling. The main features of the FeO-ZrO2 pseudo-binary system are qualitatively and quantitatively well represented. The Fe2O3/Fe3O4-ZrO2 calculated isopleth differs from the experimental one due to the presence of the Fe1O1 species in the liquid, and the excess interaction parameter between Fe1O1.5 and O2Zr1 should be refined to represent the experimental liquid miscibility gap.

At high temperatures (T > 2273 K), the ternary phase diagram is characterised by the following phase equilibria : L1 + fcc_C1, L1 + L2 + fcc_C1, L2 + fcc_C1, L2 + G, L2 + G + fcc_C1, L1 + L2 .

[1957Fis]	Fe1O1-O2Zr1 "Gleichgewichtsuntersuchungen im System Eisen(II)-oxyd-Zirkonoxyd"

Von W.A. Fischer, A. Hoffmann,

Archiv Eisenhtten, Vol.28, N°11, pp.739-743 (1957).

[1998Hel]crust

Fe1O1-O2Zr1 "The FeO-ZrO2 System"

S. Helmann, M. Nie,

In vessel cluster INV-CIT(98)-M006, IPSN/DRS/SEMAR 98/36, Minutes of the 4th CIT Project Meeting, Pisa (10th and 11th June 1998).

[1998Hel]thermocouple

Fe1O1-O2Zr1 "The FeO-ZrO2 System"

S. Helmann, M. Nie,

In vessel cluster INV-CIT(98)-M006, IPSN/DRS/SEMAR 98/36, Minutes of the 4th CIT Project Meeting, Pisa (10th and 11th June 1998).

[1999Bec]	Fe1O1-O2Zr1 "The FeO-ZrO2 System"

S. Bechta,

Private communication

[2003Gus]	Fe1O1-O2Zr1 "Phase diagram of the ZrO2-FeO system"

V. Gusarov,

Alexandrov Research Institute of Technology NITI, second CORPHAD Meeting, St Petersburg, September 17, 2003.

[2003Pil]	Fe1O1.5-O2Zr1 "The Fe3O4-ZrO2 pseudo-binary system"

P. Piluso,

Note Technique DTP/STH/LMA-03/001

[2004COR]Figure

Fe1O1-O2Zr1 "FeO-ZrO2 Phase diagram (CORPHAD measurements)"

M. Barrachin,

Private communication, october 2004.

[2004COR]VPA/IMCC

Fe1O1-O2Zr1 "System ZrO2-FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2004COR]VPA/Galakhov

Fe1O1-O2Zr1 "System ZrO2-FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2004COR]DTA

Fe1O1-O2Zr1 "System ZrO2-FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2004COR]DSC

Fe1O1-O2Zr1 "System ZrO2-FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2004COR]IMCC/EDX

Fe1O1-O2Zr1 "System ZrO2-FeO"

V.B. Khabensky et al.,

ISTC Project-1950.2 CORPHAD, NITI Progress report, October 2004.

[2004Pet]	Fe1O1.5-O2Zr1 "New miscibility gap for ex-vessel corium oxide compositions"

Y. Petrov, Y. Udalov, K. Jurek, P. Sazavski, M. Kiselova, P. Selucky, C. Journeau, P. Piluso,

Proceeding of ICAPP'04, Pittsburgh, PA USA, June 13-17, 2004, Paper 4077.

[2004Pet]1Liquid

Fe1O1.5-O2Zr1 "New miscibility gap for ex-vessel corium oxide compositions"

Y. Petrov, Y. Udalov, K. Jurek, P. Sazavski, M. Kiselova, P. Selucky, C. Journeau, P. Piluso,

Proceeding of ICAPP'04, Pittsburgh, PA USA, June 13-17, 2004, Paper 4077.

[2004Pet]estimated

Fe1O1.5-O2Zr1 "New miscibility gap for ex-vessel corium oxide compositions"

Y. Petrov, Y. Udalov, K. Jurek, P. Sazavski, M. Kiselova, P. Selucky, C. Journeau, P. Piluso,

Proceeding of ICAPP'04, Pittsburgh, PA USA, June 13-17, 2004, Paper 4077.

Figure 1  	Calculated Fe-O-Zr isothermal section at 2073.15 K.

[1965Buz]	Fe-O-Zr " "

Z. Buzek,A. Hutla,

Sbornik VSB Ostrave, (Hutuicka), 11, 383 (1965).

[1982Lia]	Fe-O-Zr "Solubility of Oxides in Liquid Alloys Containing Titanium and Zirconium",

W.W. Liang,W. Schuster,

Transactions of the Japan Institute of Metals, 23(7), 368-377 (1982).

Figure 2 	Calculated Fe-O-Zr isothermal section at 2473.15 K.

Figure 3	Calculated Fe-O-Zr isothermal section at  2773.15 K.

Figure 4	Calculated Fe-O-Zr isothermal section at  3073.15 K.

FE-U-ZR

The phase diagram of the Fe-U-Zr ternary system presents the following condensed solutions and substances, with the symbols used in this work or found in open literature :

- the liquid phase, L, which shows a complete miscibility between all elements ;

- the intermetallic Laves phase, Fe2(U, Zr)(Laves), which shows a miscibility gap at low temperature between a  Fe2U1 rich Laves phase and a Fe2Zr1 rich Laves phase ;

- the terminal iron rich solid solutions, body cubic centred, bcc_A2, and face cubic centred, fcc_A1, with a negligible solubility of uranium and a small solubility of zirconium ;

- the terminal uranium-zirconium solid solution, body cubic centred, bcc_A2, with a limited solubility of iron ;

- the terminal uranium rich solid solution, tetragonal (tet_metal), with a very small solubility of iron and zirconium ;

- the terminal uranium rich orthorhombic solid solution, ort_A20,  with a negligible solubility of iron and a very small solubility of zirconium ;

- the terminal zirconium rich solution, with the hexagonal closed packed structure, hcp_A3, and a very small solubility of iron and uranium ;

- the intermetallic solid solution, , which extents from 64 to 78 at % Zr ;

- the binary intermetallic compounds, Fe1U6(S), Fe765Zr265(S), Fe1Zr2(S) and Fe1Zr3(S) ;

- the ternary intermetallic compounds, Fe0.333U0.25Zr0.417(), Fe0.06U0.71Zr0.23(), Fe0.50U0.18Zr0.32().

The fundamental thermodynamic properties (Cp, H298, S298) of substances, Fe2U1(Laves), Fe1U6(S), Fe2Zr1(Laves), Fe765Zr265(S), Fe1Zr2(S) and Fe1Zr3(S) have been assessed in the individual sub-systems, as well as the thermodynamic modelling of all binary phases. The liquid, bcc_A2, fcc_A1, hcp_A3 phases () have been described by a non ideal substitutional model, with the formula (Fe1,U1,Zr1)(). The intermetallic Laves phase, Fe2(U,Zr)(Laves), has been described by a two-sublattice model, with the formula (Fe1, U1, Zr1)2(Fe1, U1, Zr1)1. In order to reproduce the non-stoichiometric field in the Fe-Zr binary system. The thermodynamic properties of the three ternary intermetallic compounds, Fe0.333U0.25Zr0.417(), Fe0.06U0.71Zr0.23(), Fe0.50U0.18Zr0.32() have been estimated from the phase diagram information. The gas phase has been described by an ideal mixture of gaseous species, with the formula (Fe1, U1, Zr1, Zr2)1(G).

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- the ternary intermetallic compounds are reproduced in accordance with experimental phase diagram at temperatures below 1000 K ;

- the miscibility gap in the ternary Laves phase is present up to 1373 K ;

  - above 1573 K, the only solid phases are the Fe2Zr1 rich Laves phase, the iron rich (fcc_A1, bcc_A2) and uranium-zirconium rich (bcc_A2) solution phases. Then, the liquid domain is more and more extended, pure iron melts at 1811 K, pure Fe2Zr1 at 1950 K, and pure zirconium at 2128 K. There is no available experimental information at high temperature (T > 1500 K).

Figure 1	Calculated Fe-U-Zr isothermal section at 1073.15 K.

Figure 2	Calculated Fe-U-Zr isothermal section at 1273.15 K.

Figure 3	Calculated Fe-U-Zr isothermal section at 1473.15 K.

Figure 4	Calculated Fe-U-Zr isothermal section at 1673.15 K.

O-U-ZR

The phase diagram of the O-U-Zr ternary system presents the following solutions and substances, with the symbols used in this work :

- the liquid phase, L, which shows a miscibility gap between an uranium-zirconium rich metallic liquid (L1) and a UO2-ZrO2  rich oxide liquid (L2) ; the miscibility gap is closed at high zirconium content ;

- the oxide solid solution, (U,Zr)O2+x, with the face-centred cubic structure, of CaF2 (fluorite) type, Fm3m, cF12, noted fcc_C1 ;

- the terminal zirconia rich solid solution, (U,Zr)O2, tetragonal, tet_oxide,  with a solubility of O2U1 limited to about 23 mol% ;

- the terminal uranium-zirconium rich solid solution, body cubic centred, bcc_A2, with a limited solubility of oxygen on the O-Zr side, showing a complete miscibility at high temperature and a small miscibility gap deported on the uranium side between 950 K and 1000 K in the U-Zr system ;

- the terminal zirconium rich hexagonal closed packed solid solution, hcp_A3, with a solubility of oxygen limited to about 10 at% and 30 at% respectively, and a small solubility of uranium (< 3 at%) ;

- the intermediate solid oxides, O3U1(S), O8U3(S), O9U4(S) ;

- the pure solid oxide, with the allotropic form monoclinic, O2Zr1(mon) ;

- pure solid uranium, with a negligible solubility of oxygen, and different allotropic structures, orthorhombic, U1(ort_A20), tetragonal, U1(tet) ;

- the terminal uranium rich solid solutions, orthorhombic, ort_A20, and tetragonal, tet_metal, with a small solubility of zirconium ;

- the intermetallic solid solution, , which extents from 64 to 78 at% Zr ;

- the gas phase, which shows an extended solubility of uranium above 2000 K and zirconium above 3000 K.

The fundamental thermodynamic properties (Cp, H298, S298) of substances, O3U1(S), O8U3(S), O9U4(S), O2U1(fcc_C1), O2Zr1(fcc_C1, tet, mon), have been assessed in the individual sub-systems, as well as the thermodynamic modelling of all binary or pseudo-binary phases. The liquid phase has been described by a non ideal associate model, with the formula (O1, O2U1, O2Zr1, U1,Zr1)(L). The solid solution (U,Zr)O2+x  has been described by a three sublattice model, with the formula (U1, Zr1)1(O1, □)2(O1, □)1(fcc_C1), and simplified in a simple one lattice model, with the formula (O1, O2U1, O2Zr1, U1, Zr1)1(fcc_C1), in order to be compatible with the whole thermodynamic database and to allow the introduction of iron and selected fission products, Ba, La and Sr. The terminal uranium-zirconium rich solid solutions, bcc_A2 and hcp_A3, have been described by a two sublattice model, with the respective formula (U1, Zr1)1(O1, □)3(bcc_A2), and (U1, Zr1)1(O1, □)0.5(hcp_A3). The gas phase has been  described by an ideal mixture of gaseous species, with the formula (O1, O1U1, O1Zr1, O2U1, O2Zr1, O2, O3, O3U1, U1, Zr1, Zr2)1(G).

The comparison of the calculated thermodynamic properties and phase diagram with the experimental information leads to the following conclusions :

- on a qualitative point of view, the overall topology of the O-U-Zr ternary phase diagram is in agreement with the experimental data between 1273 K and 3173 K ;

- on a quantitative point of view, the solubility of oxygen in uranium-zirconium liquid alloys, the liquid miscibility gap and the liquidus temperatures are in agreement with the selected experimental data ;

- the remaining uncertainties are the accurate shape of the diphasic domain L1 + fcc_C1 between 2000 K and 2500 K,  the liquidus temperatures in the zirconium rich domain, the solidus temperatures, and the presence of an hyper-stoichiometric liquid at low temperatures, resulting from necessary improvement of the hyper-stoichiometric O-U region.

Figure 1	Calculated O-U-Zr isothermal section at 1773.15 K.

[1975Pol]F+T+H

[1975Pol]F+H+L

[1975Pol]H+L+B

"Untersuchungen in dreistoffsystem uran-zirkon-sauerstoff"

C. Politis

Kernforschungszentrum Karlsruhe, KFK 2167, 1-53 (1975).

Figure 2	Calculated O-U-Zr isothermal section at 2773.15 K.

[1970Jun]L

[1970Jun]L+F

[1970Jun]F

"Untersuchungen in dreistoffsystem uran-zirkon-sauerstoff"

E.F. Junke and J.F. White

GEMP-731 (1970).

[1975Pol]L

[1975Pol]L+F

"Untersuchungen in dreistoffsystem uran-zirkon-sauerstoff"

C. Politis

Kernforschungszentrum Karlsruhe, KFK 2167, 1-53 (1975).

[1984Sko]L

"On the reaction between UO2 and Zr"

A. Skokan

5th Int. Meeting "Thermonuclear reactor safety", Karlsruhe (september 9-13 1984).

[1996Mau]L/L+F

"Experimental determination of the liquidus L/(U,Zr)O2-x in the (U,Zr,O) system at 2273K"

A Maurisi, C. Gueneau, P. Perodeaud, B. Schneider, O. Dugne, F. Valin and G. Bordier, Euromat (October 1996)

Figure 3	Calculated O-U-Zr isothermal section at 2773.15 K.

[1997Gol]L1+L2

"DPEA/SPEA Experiments"

S. Golstein et al.

Private communication, 1997

[1998Gue]L1+L2

"DPEA/SPEA Experiments"

C. Gueneau, V. Dauvois, P. Pérodeaud, C. Gonella, O. Dugne,

Journal of Nuclear Materials, 254 (1998) 158.

[1999Far]L

[1999Far]L+F

[1999Far]L/L+F

"Final report on severe accident material property measurements,"

M.T. Farmer, L.M. McUmber, R.W. Aeschlimann and B.W. Spencer,

ANL-NT TECHNICAL MEMORUNDUM N° 88, October 1998.

[1996Hay]L/L+F

"Dissolution of UO2 in molten zircalloy-4 :

Part3 : solubility from 2000 to 2500°C.

Part 4 : phase evolution during dissolution and cooling of 2000 to 2500°C specimens"

P.J. Hayward and I.M. George

Journal of Nuclear Materials, 232, 1, 1-22 (1996)

[2001Pun]F

[2001Pun]F/F+L

"AEAT"

AEA,

ENTHALPY Private communication

Figure 4	Calculated O-U-Zr isothermal section at 3173.15 K.

[1997Gol]L1+L2

"DPEA/SPEA Experiments"

S. Golstein et al.,

Private communication, 1997

[1998Gue]L1+L2

"DPEA/SPEA Experiments"

C. Gueneau, V. Dauvois, P. Pérodeaud, C. Gonella, O. Dugne,

Journal of Nuclear Materials, 254 (1998) 158.

[1999Far]L

"Final report on severe accident material property measurements,"

M.T. Farmer, L.M. McUmber, R.W. Aeschlimann and B.W. Spencer,

ANL-NT TECHNICAL MEMORUNDUM Nø 88, October 1998.

[2001Pun]L

"AEAT"

AEA,

ENTHALPY Private communication

NOTE

Tout rapport, publication ou autre forme de document écrit

faisant appel aux résultats de cette étude,

devra obligatoirement en mentionner l'origine :

THERMODATA

[ January 2006 ]

6, rue du Tour de l’Eau - 38400 SAINT MARTIN D'HERES – France

Clause de non-responsabilité

Notre objectif est de diffuser des informations de qualité, exactes et à jour.

Toutefois, THERMODATA n’assume aucune responsabilité

quant aux informations que contient le présent document

et à l’utilisation qui pourrait en être faite.